## Slide 1: Crystal field in multielectron ions
Marie-Anne ARRIO
CNRS / Sorbonne Universite (Paris)
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 2: Crystal field
Introduction / Definition
One electron (3d electron)
  Symmetries
  Hamiltonian
  Crystal field splitting of 3d electron
Multi-electrons ion (3d electrons)
  Hamiltonian
  Configurations/ spectroscopic terms
  Symmetry
  Exemples
Crystal field and magnetism
  Hamiltonian
  Magnetic moment (spin and orbit)
  Zeeman effect / paramagnetism
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 3: Crystal field : origin
Hans Bethe (1906-2005)
(Nobel Prize in Physics 1967)
In 1929 (University of Tübingen): Model to explain the properties of NaCl crystal.
Ions are considered to be undeformable charged spheres and the interaction between them simply results from the electric potential generated by these charges.
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 4: Crystal field : origin
Cl-
Na+
NaCl crystal
Na+ ion surrounded by 6 Cl- ions as nearest neighbors
• Ions = indeformable charged spheres
• Interaction results from the created electrostatic potential
Electrostatic potential produced by a negative charge:
(r = distance between the centered charge and a point i)
Effect of the 6 negative charges:
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 5: Crystal field : origin
Analogy for solid-state or coordination complex
Consider the ligands and the metal as charged spheres
Na+ ≈ metal ion - Cl- ≈ ligand
Perovskite SrTiO3
O2-
Ti4+
Fe3+
CN-
Tp=tris-pyrazolyl borate
Tp-

## Slide 6: Symmetries
Symmetry is responsible for many physical and spectroscopic properties of compounds
Group theory is a powerfull tool, which not only allows one to simplify calculations, but also defines the language of labeling states and can predict without calculations if states couple under certain interactions or if certain transitions are allowed or not.
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 7: Symmetry operations : some notations to know
E, the identity
Cn, a rotation by an angle 2π/n;
σ reflection in a plane, classified as
  σh,reflectionthroughaplaneperpendiculartotheaxisofhighestrotationsymmetry, called principal axis
  σv, reflection through a plane to which the principal axis belongs
  σd, reflection through a plane to which the principal axis belongs, and bisecting the angle between the two-fold axes perpendicular to the principal axis.
Sn = σh ⊗Cn, improper rotation of an angle 2π/n
I = S2, the inversion.
Quanty mathematica : Quanty/guide/PointGroupSymmetry

## Slide 8: Symmetries : some point groups
Each group has a table of representations
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 9: Symmetries : Oh
O2-
Ti4+
Octahedral
Group : Oh
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 10: Crystal field hamiltonian and symmetry
All you need is in the web page Quanty.org
http://quanty.org/physics_chemistry/point_groups
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 11: Crystal field hamiltonian and symmetry
http://quanty.org/physics_chemistry/point_groups/oh
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 12: Symmetries
O2-
Ti4+
Trigonal
Group : C3v
Fe3+
CN-
Tp-
Octahedral
Group : Oh
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 13: Crystal field hamiltonian
The crystal field potential can be expanded on the normalized spherical harmonics
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 14: Crystal field hamiltonian
The crystal field potential can be expanded on the normalized spherical harmonics
Where to stop the expansion over k ?
Writing the CF matrix element on the basis functions. Depends on :
The crystal field Hamiltonian thus writes
with l the orbital momentum of the shell (2 for 3d ions, 3 for 4f ions)
(hermician hamiltonian)
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 15: Crystal field hamiltonian and symmetry
Not all values of Akm are allowed :
many are zero due to the local symmetry of the ion
Symmetry related:
For all symmetry operation (Oi) of the point-group G, we have
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 16: Crystal field hamiltonian and symmetry
Not all values of Akm are allowed : many are zero due to the symmetry around the ion
For all symmetry operation (Oi) of the point-group G,
Only one non-zero Akm : A40
Oi
Example : Oh symmetry
http://quanty.org/physics_chemistry/point_groups/oh
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 17: Notations for crystal field parameters
The notations vary a lot from an author to the other
(Haverkort/QUANTY)
And symmetry dependent parameters like (Balhausen, König, Kremer,..)
10Dq for cubic
{10Dq, Ds, Dt} for tetragonal symmetry D4h
…. etc.
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 18: Crystal field
Introduction / Definition
One electron (3d electron)
  Symmetries
  Hamiltonian
  Crystal field splitting of one 3d electron
Multi-electrons ion (3d electrons)
  The spherical ion :
  Crystal field
  Core hole spectroscopy : examples
Crystal field and magnetism
  Hamiltonian
  Magnetic moment (spin and orbit)
  Zeeman effect / paramagnetism
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 19: 3d transitions metal ions
In material made of 3d transitions metal ions, a lot of physico-chemical properties are due to the crystal field
For example
Color
Magnetic properties
Ni2+
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 20: One electron function : Orbital
Basis of atomic orbitals
Radial part
Angular part
Spherical harmonics
Spin part
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 21: 3d atomic orbitals
Basis of atomic orbitals
3d shells : n=3, l=2 2l+1=5 basis functions ( -2 ≤ l ≤ 2 )
3d orbitals are real functions, linear combination of
x
y
z
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 22: Oh crystal field splitting of 3d electron
Matrix elements
Diagonalization
CF matrix in {Y2,m} basis=
Oh crystal field splits the d orbitals in two groups of orbitals
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 23: Oh Crystal field splitting of 3d electron Use of group symmetry
From the Oh group properties, one could have guessed the splitting of the d orbitals
d orbitals are called eg and t2g *
(*)N.B. : lower case letter (eg and t2g) for one electron
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 24: Oh Crystal field splitting of 3d electron Parameters
From diagonalization
adjustable parameter
Towards the ligand : destabilized
Towards the ligand :
stabilized
In QUANTY, the Ak,m are defined in function the orbital energies (can be modified)
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 25: Tetragonal (D4h) crystal field splitting of 3d electron
Elongated
or compressed Oh
along C4 axis
Square planar
D4h
From the D4h table, one can predict the 3d splitting in 4 groups
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 26: Tetragonal (D4h) crystal field splitting of 3d electron
The CF matrix is diagonal in the {d} basis and the energies are :
with
The relation with Dq,Ds,Dt can be found in the book of König&Kremer « Ligand field. Energy diagram »
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 27: Tetragonal (D4h) crystal field splitting of 3d electron
10Dq
10Dq
D4h (elongation)
Oh
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 28: Crystal field hamiltonian in QUANTY
Akm = PotentialExpandedOnYlm("Oh",2,{0.6,-0.4});
OpptenDq = NewOperator("CF", NFermion, dIndexUp, dIndexDn, Akm);
The Oh potential is defined by:
1) Pre-defined CF potential
1) User made CF potential: Akm=
Akm = {{4,0,21/10},{4,-4,21/10sqrt(5/14)}, {4,4,21/10sqrt(5/14)}};
OpptenDq = NewOperator("CF", NFermion, dIndexUp, dIndexDn, Akm);
The parameter is 10Dq and the hamiltonian writes
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 29: Crystal field
Introduction / Definition
One electron (3d electron)
Multi-electrons ion (3d electrons)
  The spherical ion :
    Configuration
    Hamiltonian
    |(L,S),J> basis function
    Spectroscopic terms
  Crystal field
    Basis functions, hamiltonian and matrix element
    Energy diagram (Tanabe-Sugano)
  Core hole spectroscopy : examples
    Spin cross-over
    The limit of the crystal field model : towards ligand field
Crystal field and magnetism
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 30: Multi-electrons ions : configuration
Electronic configuration: complete simplified (open shell)
3d transition metal ions 1s22s22p6 3dn 3dn
4f rare earth ions 1s22s22p63s23p63d10 4fn 4fn
Example of term splitting
Many possibility of filling of the 3d orbitals
2l+1=5 |l,ml> angular functions
2s+1=5 |sms> spin functions
Nb states = Cn10 =
Degeneracy = multiplets
ml=-2 -1 0 1 2
10 functions
Example of a d2 system (V3+, Cr4+) :
degenerate states : C210 = 45
Some possibilites:

## Slide 31: Multi-electrons ions configuration and symmetry
d2 ion in Oh symmetry
eg
t2g
Orbital degeneracy
Spin degeneracy
3
1 (S=0)
3x2=6
1 (S=0)
3x2=6
3 (S=1)
6
1 (S=0)
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 32
Hion = Hcin + He-n + He-e + Hs-o + HCF
Free ion (spherical)
Crystal field
Total kinetic energy
Coulomb attraction nuclei-electrons
Electron-electron Coulomb repulsions
Spin-orbit coupling
Hamiltonian of the ion with N electrons

## Slide 33
Hamiltonian of the ion with N electrons
Multi-electron functions for N electrons
Y(r1,r2,...,rN)
Linear combination of Slater determinant built from the mono-electronic functions
Anti-symmetric function to satisfy the Pauli principle
Basis functions |Y>

## Slide 34
Ion with N electrons : operators
somme  couplage d’opérateurs
!
!
Sum is coupling

## Slide 35
Free ion with N electrons : basis functions
Fonctions |a(L,S)JMJ>
Common eigenfunctions with
(Hcin+He-n+He-e commute with )
Hcin+He-n+He-e+Hs-o commute with
The energy of |a(L,S)JMJ> does not depend on MJ
Degeneracy of |a(L,S)JMJ> = 2J+1
35
letter for L
G=S pour L=0
G=P pour L=1
G=D pour L=2
G=F pour L=3
S spin
Spectroscopic terms |a(L,S)JMJ> =
2S+1 LJ
The energy of |a(L,S) > does not depend on ML, MS
Degeneracy of |a(L,S)> = (2L+1)(2S+1)

## Slide 36: Free ion : spectroscopic terms for 3d2 ion
Split the 5 LS terms into 9 (L,S)J terms :
*only diagonal energy corrections here (neglect off diagonal coupling with other LS terms)
Landé interval rule
Ground state given by
Third Hund’s rule
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 37: Crystal field : basis function
Basis functions
Spherical symmetry:
|a(L,S) J MJ>
Local symmetry around the ion  point group G:
Basis functions of the representations of group G
|a(L,S) J G g >
G irreducible representation of G
Gg basis function of G
Thole’s code uses group theory and the {G} basis (TTMULT, CTM4XAS)
QUANTY
  uses group theory only for crystal field potential building
  does not use the {G} basis
  uses {G} to label the states (spectroscopic terms)
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 38: Crystal field and group theory
Free ion
O3 is the group of the sphere
|a(L,S) J MJ> partners of irrep* J of O3
Ion in solid/molecule
G is the subgroup of the sphere
|a(L,S) J G g > partners of the irrep* G of G
Hamiltonian expanded on Ck,m
Hamiltonian expanded on Ck,m
and invariant over the symmetry operation of G
* irrep=irreducible representation
Ex: Oh symmetry
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 39: Crystal field and group theory Matrix elements
(fully symmetric representation of group G)
* g only for centro-symmetric group
if
Crystal field mixes J states if
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 40
Ex: d1 (d9) ion in Oh symmetry
L=2
S=1/2
J=3/2,5/2
eg
t2g
eg
t2g
O3
Oh
2Eg
2T2g
Orbitals
O3
2D
2T2g
2Eg
U’
U’
E’’
2D3/2
2D5/2
O3
+spin-orbit
Oh
Oh
+ spin-orbit
J states mixed by CF and SO
States (spectroscopic terms)

## Slide 41: Crystal field and group theory
Free ion
O3
Oh
Example of d2 ion in Oh symmetry
Crystal field splitting of the ground state
From the group branching table (Butler)
eg
t2g
eg
t2g
eg
t2g
Oh
strong field
From the multi-electronic state, one can get the electron density on the orbitals of the group (it is not necessary integer)
(spin-orbit omitted for simplicity)
Simplified
orbital scheme
!
45 states
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 42: Crystal field : energy diagram
Plot of the energy of spectroscopic terms
as function of crystal field parameter (10Dq,Ds,…) (and B Racah parameter (*))
Tanabe-Sugano diagram (1954) König&Kremer (≈1970)
Oh(Td) , no spin-orbit Low symmetries+spin-orbit
(*)B Racah parameters related to the slater integrals (electronic repulstions)
d2
3T1g
3F
3A2g
3T2g
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 43: Crystal field : energy diagram
Plot of the energy of spectroscopic terms
as function of crystal field parameter (10Dq,Ds,…) (and B Racah parameter (*))
Tanabe-Sugano diagram (1954) König&Kremer (≈1970)
Oh(Td) , no spin-orbit Low symmetries+spin-orbit
Tutorial Monday afternoon :
02_Energy_Level_Diagram_Tanabe-Sugano.Quanty
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 44: Crystal field : multi-electron and orbitals
Multi-electron ions
One electron/orbitals
Spectroscopic terms :
Term written with capital letter in Müliken notation. Ex :
or Koster notation :
Electron density / orbitals
ex :
L,S,J,ML,MS,MJ not « good » quantum numbers.
Expectation values:
Orbitals :
Small letter
ex:

## Slide 45: Multiplet, crystal field applied to core hole spectroscopies
Calculations including the core-hole (ex : 2p53dn+1, 3d94fn+1,…) and many kind of transitions (electric dipole, magnetic dipole…)
RACAH/BANDER, Thole’s code : core of CTM4XAS (Frank de Groot)
Based on group theory (Butler “Point group symmetry applications”)
Difficult to modified and adapt to new spectroscopies since Theo Thole died in1996
QUANTY, Haverkort’s code
Flexible for the need of the new spectroscopies/physical properties
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 46: Example of crystal field : spin crossover
T = 300K S = 2
High spin
T = 77K S = 0
Low spin
L3
L2
FeII(phen)2(NCS)2
Absorption (a.u)
spin crossover
a well known crystal field effect
intensively studied and observed with many different spectroscopies and magnetic measurements
Ex : XAS at L2,3 edges
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 47: Crystal field effect : spin crossover
Fe2+ ion (3d6) in Oh symmetry
When 10Dq increases, the ground state changes
eg
t2g
eg
t2g
S=2
High spin
S=0
Low spin
The magnetic properties goes from paramagnetic to non-magnetic
Good candidate for many applications like molecular spintronic
10Dq
Energy/B
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 48: Crystal field effect : spin crossover XAS at Fe L2,3 edges (2p->3d)
Fe2+ ion (3d6) in Oh symmetry
When 10Dq increases, the ground state changes
eg
t2g
S=2
High spin
eg
t2g
S=0
Low spin
Experiment
Calculations
10Dq=1eV
10Dq=2.2eV
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 49
(covalent) CrIII-CN-NiII (ionic)
Limit of the crystal field model: towards ligand field model
Example : prussian blue analogues
CsI[NiIICrIII(CN)6].xH2O
CrIII
NiII

## Slide 50
Weak covalent bond
CN-NiII in Cs[NiCr(CN)6]
L3
L2
Oh crystal field 10Dq = 1.4 eV
(  optical spectro.)
k = 0.8 (weak covalent bond)
NiII L2,3 edges (2p to 3d)
CrIII
NiII
experiment
Calculation
d8 Oh

## Slide 51
Weakness of crystal field theory
Strong crystal field
Arrio et al. J. Am. Chem. Soc. 1999, 121, 6414-6420.
CrIII L2,3 edges
Exp.
k = 0.5
CrIII
NiII
experiment
Crystal field calc.
Ligand field calc.
Crystal field : Oh, large 10Dq (=3.5eV) + strong slater reduction (50%)
Incomplete model due to the strong metal to ligand charge transfer
Ligand field : metal to ligand charge transfer
d3d0 + d2d1

## Slide 52: Crystal field and magnetism
Hamiltonian
Magnetic moment (spin and orbit)
Zeeman effect / paramagnetism
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 53: External magnetic field effect : Zeeman effect
Hion = Hcin + He-n + He-e + Hs-o + HCF +HZeeman
Free ion (spherical)
Crystal field
Splitting of states that depends on (mL,mS)
Matrix element depend on the magnetic moment
Hamiltonian
d1 S=1/2
mS=+1/2
mS=-1/2
1 electron (S=1/2)
spherical
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 54: Magnetic moments
|(L,S)J Gg> (G term) are not eigenfunctions of
Linear combination of mL
Definitions
Crystal field effect:
For 3d ions, the orbital magnetic moment is quenched (nul) in most cases.
Some 3d ions have significant orbital magnetic moment (Co2+, low spin Fe3+, Fe2+)
 atomic magnetic anisotropy
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 55: Magnetic moments and spectroscopies
More operators involved like Tz (magnetic sum rules)
Magnetic spectroscopies : XMCD, RIXS-MCD, XMLD
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 56: Magnetic moments in QUANTY
QUANTY any operator ( ) and its expectation values
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 57: Magnetic moments in QUANTY
QUANTY any operator ( ) and its expectation values
Ex : spin operator
Tutorial 07_Expectationvalues.Quanty
(Monday morning)
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 58: Magnetization of paramagnetic 3d ion (Zeeman effect)
Magnetic moment of state
Magnetic moment at temperature T in the magnetic field Hz
With Z the partition function
Magnetization curve for a paramagnetic ion
Hz(tesla)
Co2+ (d7) Oh (QUANTY)
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 59: Conclusion / remarks
It can be difficult and sometime false to use a single electron model for the multi-electron ion
Other {d} basis than {dxy,dxz,dyz,dz2,dx2-y2} can be chosen for complex symmetries (ex: C3v, D5d)
Crystal field is an empirical model (parameter dependent) but it can be linked to more ab-initio methods (tight-binding, DFT, CASSCF,… )
Lecture: Maurits Haverkort
Crystal field will make angular dependences in transitions
Lecture : Amélie Juhin
Crystal field affect the magnetic properties of 4f rare earth ions (not discussed here)
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 60: Appendix
Notes: One electron :
symmetry : small letters for notation eg, a1g

## Slide 61: Naming point groups:
The name of the point group has information about the symmetry elements present. The letter is the rotational group and the subscript number after the letter indicates the order
of the principal rotational axis (e.g. 3-fold or 4 fold etc.):
C3 C3v D4d D4h
A ‘C’ indicates only one rotational axis
A ‘D’ indicates an n-fold
principal rotation axis
plus n 2-fold axes at
right angles to it
3-fold rotational has σv but 4-fold d = no ‘h’ indicates
axis no σh mirror principal σh mirror a σh mirror
planes in a C group axis plane plane

## Slide 62: Naming point groups (contd.):
A subscript ‘h’ means that there is a σh mirror plane at right angles to the n-fold principal axis:
D4h
C4 principal axis
σh
C3 principal axis
σv
A subscript ‘d’ (or v for C groups) means there is no σh mirror
plane, but only n σv mirror planes containing the principal Cn axis.
only one
of the three
σv planes
is shown
D3d

## Slide 63: Naming platonic solids:
Platonic solids:
T = tetrahedral = 4 three-fold axes
O = octahedral = 3 four-fold axes
I = icosahedral = 6 five-fold axes
Td Oh Ih
C60
‘bucky-ball’
or ‘Fullerene’

## Slide 64: Magnetic sum rules for XMCD at 3d L2,3 edges
Number of 3d electrons (3dn)