## Slide 1
Introduction to XAS
XAS detection techniques
XAS spectral shape
multiplet calculations
X-ray Absorption Spectroscopy

## Slide 2
Element specific
Sensitive to low concentrations
Applicable under extreme conditions
SPACE: Combination with x-ray microscopy
TIME: femtosecond XAS
RESONANCE: RIXS, RPES, R diffraction
X-ray Absorption Spectroscopy
Notes: XAS is element specific because each element has specific binding energies for its core levels.
The XAS edge energy is essentially given by the core level binding energy.

## Slide 3: Interaction of x-rays with matter
Photo-electric (X-ray annihilation)
Elastic X-ray scattering
Inelastic X-ray scattering
Mn
X-ray Absorption Spectroscopy

## Slide 4
Label
Orbital
eV
K
1s
6539
L I
2s
769.1
L II
2p1/2
649.9 [3]
L III
2p3/2
638.7 [3]
M I
3s
82.3 [3]
M II
3p1/2
47.2 [3]
M III
3p3/2
47.2 [3]
X-ray absorption edges
X-ray Absorption Spectroscopy

## Slide 5
Label
Orbital
eV [literature reference]
K
1s
6539 [1]
L I
2s
769.1 [3]
L II
2p1/2
649.9 [3]
L III
2p3/2
638.7 [3]
M I
3s
82.3 [3]
M II
3p1/2
47.2 [3]
M III
3p3/2
47.2 [3]
X-ray absorption edges
X-ray Absorption Spectroscopy
BarKLa
The Nobel Prize in Physics 1917 was awarded to Charles Glover Barkla "for his discovery of the characteristic Röntgen radiation of the elements."

## Slide 6
Label
Orbital
eV [literature reference]
K
1s
6539 [1]
L I
2s
769.1 [3]
L II
2p1/2
649.9 [3]
L III
2p3/2
638.7 [3]
M I
3s
82.3 [3]
M II
3p1/2
47.2 [3]
M III
3p3/2
47.2 [3]
X-ray absorption edges
X-ray Absorption Spectroscopy
sharp
principal
diffuse
fundamental
BarKLa
The Nobel Prize in Physics 1917 was awarded to Charles Glover Barkla "for his discovery of the characteristic Röntgen radiation of the elements."
J. Chem. Educ. 84, 757 (2007)

## Slide 7
X-ray absorption
X-ray Absorption Spectroscopy
Excitation of 3p to 3d state
Lifetime of excitation is short
Lifetime broadening ~200 meV
4sp
3d
O2p
O2s
3p
Notes: 7

## Slide 8
X-ray absorption & x-ray emission
X-ray Absorption Spectroscopy
Decay of 3d electron to 3p core state
X-ray emission
Notes: 8

## Slide 9
X-ray absorption & Auger
Decay of 3d/valence electron to 3p core state
Energy used to excite a 3d/valence electron
Auger electron spectroscopy
X-ray Absorption Spectroscopy
Notes: 9

## Slide 10
X-ray Absorption Spectroscopy
1s core state
Notes: 10

## Slide 11
XAS: detection techniques

## Slide 12
Use decay channels as detector
XAS: detection techniques
Uniform thickness
Uniform concentration of absorbing element
Thin enough for photons

## Slide 13
X-ray penetration lengths &
electron escape depths
100-1000 nm
(CXRO, but 20 nm for L edges)
1-5 nm
XAS: detection techniques

## Slide 14
Use decay channels as detector
XAS: detection techniques
X-ray penetrate 1000 nm (λX)
Electrons escape from 5 nm (λE)
Number of core holes created in first 5 nm is proportional to μ and angle of incidence (α)
ITEY ~ 1 / λX = μX

## Slide 15
Transmission
(pinhole, saturation > thin samples)
Electron Yield
(surface sensitive)
Fluorescence Yield
(saturation & self-absorption:
> dilute samples)
[L edges are intrinsically distorted]
XAS: detection techniques

## Slide 16
Interpretation of spectral shapes
XAS: spectral shape
Notes: 16

## Slide 17
Excitations of core electrons to empty states
The XAS spectra are given by the Fermi Golden Rule
XAS: spectral shape
exciton
edge jump

## Slide 18
Fermi Golden Rule

Excitations to empty states as calculated by DFT
O 1s
XAS: spectral shape (O 1s)
X
Notes: 18

## Slide 19
2p
2s
Phys. Rev. B.40, 5715 (1989)
XAS: spectral shape (O 1s)

## Slide 20
Phys. Rev. B.40, 5715 (1989); 48, 2074 (1993)
XAS: spectral shape (O 1s)
oxygen 1s > p DOS

## Slide 21
Phys. Rev. B. 40, 5715 (1989); 48, 2074 (1993)
XAS: spectral shape (O 1s)

## Slide 22
Final State Rule: Spectral shape of XAS looks like final state DOS
TiSi2
Phys. Rev. B. 41, 11899 (1991)
XAS: spectral shape

## Slide 23
XAS codes:
Multiple scattering: FEFF, FDMNES, etc.
Band structure: WIEN2K, Quantumespresso, etc.
Real-space DFT: ADF, etc.
TiSi2
Phys. Rev. B. 41, 11899 (1991)
XAS: spectral shape

## Slide 24
Iron 1s XAS
2p XAS of transition metal ions
[Phys. Rev. B. 42, 5459 (1990)]
exciton
edge jump
2p > s,d DOS
2p > 3d
(3d5 > 2p53d6, self screened)
X
Notes: 24

## Slide 25
2p3/2
2p1/2
Overlap of core and valence wave functions
 Spectral shape NOT improved in last 30 years!
3d
<2p3d|1/r|2p3d>
XAS: multiplet effects
XAS: spectral shape
[Phys. Rev. B. 42, 5459 (1990)]

## Slide 26
1-particle:
1s edges
(DFT + core hole +U)
many-particle:
open shell systems
(CTM4XAS)
Interpretation of XAS
XAS: spectral shape
Notes: 26

## Slide 27
XAS
1s
DFT
pre-edge
of 3d system
2p, 3p,
3d, 4d
multiplets
XAS: spectral shape

## Slide 28
Charge Transfer Multiplet program
Used for the analysis of XAS, EELS,
Photoemission, Auger, XES involving d and f-shells
ATOMIC PHYSICS

GROUP THEORY

MODEL HAMILTONIANS
CHARGE TRANSFER MULTIPLETS
Notes: The TT-multiplets program can be used to explain the spectral shapes of all core level spectroscopies. XAFS, photoemission, auger, etc.
The program combines three advanced computer codes, an atomic physics code to describe all atomic interactions, a group theory code to describe the local symmetry (think of crystal fields) and model Hamiltonians to describe many body effects correlated systems.
AS A SIDE REMARK I WOULD LIKE TO MENTION that the active site in a catalyst is a perfect example of a correlated system. (in biocatalysis this is often realised)
The integrated program gives accurate descriptions of core level spectra, from a set of uniform electronic structure parameters.
The program is important for all of the new spectroscopies that I will describe.
The program is distributed from my homepage and it is used at some 50 institutes worldwide.

## Slide 29
Atomic Multiplet Theory
=E
Kinetic Energy
Nuclear Energy
Electron-electron interaction
Spin-orbit coupling
ATOMIC MULTIPLETS

## Slide 30
Atomic Multiplet Theory
X X
=E
Kinetic Energy
Nuclear Energy
Electron-electron interaction
Spin-orbit coupling
ATOMIC MULTIPLETS

## Slide 31
ATOMIC MULTIPLETS 3d1
5 orbitals (each spin-up or spin-down) >> total 10 states
No electron-electron interaction: all states have the same energy
Quantum numbers: L=2 and S=½, notation as term symbol: 2S+1L= 2D

## Slide 32
ATOMIC MULTIPLETS 3d1
Spin-orbit coupling couples L and S quantum numbers to a total quantum number J
Jmax= L+S = 5/2, Jmin= |L-S|= 3/2, Integer steps of J.
Two term symbols: L=2, S=½, and J = 5/2 >> notation as term symbol: 2S+1LJ= 2D5/2
L=2, S=½, and J = 3/2 >> notation as term symbol: 2S+1LJ= 2D3/2

## Slide 33
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d1
3d1
2D
2D3/2
2D5/2
electron-electron
interaction
spin-orbit
coupling
(~50 meV)

## Slide 34
ATOMIC MULTIPLETS 3d2
5 spin-up orbitals give 4 + 3 + 2 + 1 = 10 paired 3d2 states
5 spin-down orbitals give 10 paired down-down 3d2 states
There are 5x5 = 25 up-down states
In total 10+10+25 = 45 states
Can also be calculated as 10 x 9 / 2 = 45 states
Electron-electron interaction is different for different orbital combinations
There will be a number of different states with different energies.
Analysis shows that the states are 1S, 3P, 1D, 3F and 1G

## Slide 35
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d2
3d2
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
electron-electron
Interaction
(~2 eV)
spin-orbit
coupling
(~50 meV)
    Ground state:
    Given by Hunds rules
    max S
    max L
    min J (if less than half full)

## Slide 36
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d8
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
electron-electron
Interaction
(~2 eV)
spin-orbit
coupling
(~50 meV)
    Ground state:
    Given by Hunds rules
    max S
    max L
    max J (if more than half full)

## Slide 37
Atomic Multiplet Theory
X-ray absorption from 3d8 to 2p53d9
2p53d9
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
Dipole selection rule:
ΔJ=-1, 0 or +1

## Slide 38
Atomic Multiplet Theory
X-ray absorption from 3d8 to 2p53d9
2p53d9
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
Dipole selection rule:
ΔJ=-1, 0 or +1

## Slide 39
Atomic multiplets
2p XAS of NiO with atomic multiplets

## Slide 40
3d XAS of rare earths
4f electrons are localized
No effect of surroundings (crystal field < lifetime broadening)
3d XAS is self screened > no charge transfer effect
Initial state
electron-electron interaction.
Valence spin-orbit coupling
Final state
+ core hole – valence hole ‘multiplet’ interaction.
+ core hole spin-orbit coupling

## Slide 41
3d XAS of rare earths
Nd3+ 4f3 system: ground state is 4I9/2

## Slide 42
Atomic multiplets
2p XAS of NiO with atomic multiplets

## Slide 43
2p XAS of 3d transition metal oxides
3d electrons are less localized
Effect of surroundings (crystal field effect)
3d XAS is self screened > weak charge transfer effect
Initial state
electron-electron interaction.
valence spin-orbit coupling
crystal field effect
Final state
core hole – valence hole ‘multiplet’ interaction.
core hole spin-orbit coupling
crystal field effect

## Slide 44
t2g states
Crystal Field Effects
eg states
crystal field effect

## Slide 45
High-spin or Low-spin
E
T2
E
T2
High-spin 3d5
Low-spin 3d5
crystal field effect: spin state
More in the lecture of Marie-Anne Arrio

## Slide 46
valence e-e interactions Fdd
core-valence e-e Fpd Gpd
core & valence spin-orbit ζ
crystal field 10Dq, Ds, Dt
molecular field, M or H
e-e screening κ
charge transfer Δ, U, Q
hopping TΓ
ionic 3d
(4d, 5d)
4f, 5f
covalent 3d
mixed valence f
ATOMIC
SYMMETRY
BONDING
Multiplet calculations

## Slide 47
valence e-e interactions Fdd
core-valence e-e Fpd Gpd
core & valence spin-orbit ζ
crystal field 10Dq, Ds, Dt
molecular field, M or H
e-e screening κ
charge transfer Δ, U, Q
hopping TΓ
ionic 3d
(4d, 5d)
4f, 5f
3d ions
covalent 3d
mixed valence f
ATOMIC
SYMMETRY
BONDING
Multiplet calculations

## Slide 48
Hubbard U for a 3d8 ground state:
U= E(3d7) + E(3d9) – E(3d8) – E(3d8)
Ligand-to-Metal Charge Transfer (LMCT):
= E(3d9L) – E(3d8)
Charge Transfer Effects
Charge transfer effects

## Slide 49
Charge Transfer Effects
Main screening mechanism in XAS of oxides:
Ligand-to-metal charge transfer
Charge transfer energy  is important for XAS
Hubbard U is NOT important for XAS spectral shape
Charge transfer effects

## Slide 50
3d9L
Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

3d8
Ground State
Charge transfer effects in XAS and XPS
transition metal oxides

## Slide 51

Charge Transfer Effects
3d8
3d9L

## Slide 52

Charge Transfer Effects
3d8
3d9L
9
8

## Slide 53
β 3d8 - α 3d9L
α 3d8 + β 3d9L

Charge Transfer Effects
3d8
3d9L

## Slide 54
E1,2 = ½ [±√(2+4T2)]
=2 and T=0
E1,2 = ½ [2±√(22+0)] = 0 and 2

Charge Transfer Effects
3d8
3d9L

## Slide 55
E1,2 = ½ [±√(2+4T2)]
=2 and T=1
E1,2 = ½ [2±√(22+4)] = 1 ± √2

Charge Transfer Effects
3d8
3d9L

## Slide 56
Charge Transfer Effects in NiO
E(3d9L) – E(3d8) = 
E(3d10LL‘) – E(3d8) = 2
X

## Slide 57
Charge Transfer Effects in NiO
E(3d9L) – E(3d8) = 
E(3d10LL‘) – E(3d8) = 2 +U

## Slide 58
Charge Transfer Effects

## Slide 59

+U-Q
Charge Transfer Effects in XAS

## Slide 60
3d9L
3d8
NiO: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

2p53d10L
2p53d9
+U-Q  
Charge Transfer Effects
Charge transfer effects

## Slide 61
β 3d8 - α 3d9L
α 3d8 + β 3d9L

+U-Q  
β’ c3d9 – α’ c3d10L
α' c3d9 + β’ c3d10L
~0
~1
Intensity bonding combination: [α α’+ β β’]2
α  α’  (α2+ β2)2 =1
Charge transfer effects

## Slide 62
β 3d5 - α 3d6L
α 3d5 + β 3d6L

+U-Q  
β’ c3d6 – α’ c3d7L
α' c3d6 + β’ c3d7L
~0
~1
Intensity anti-bonding combination: [α β’- β α’]2
α  α’  (αβ – βα)2 =0
Charge transfer effects

## Slide 63
Neutral experiments are self-screened
XAS, optical, EPR, EELS, RIXS
>> small screening satellites
>> crystal field theory can be used
Ionising experiments are not self-screened
XPS, Auger,
>> large screening > large satellites
>> crystal field theory can not be used
Charge Transfer Effects
Charge transfer effects

## Slide 64
3d6L
Transition metal oxide: Ground state: 3d5 + 3d6L
Energy of 3d6L: Charge transfer energy 
XAS
2p53d7L
+U-Q  

2p53d6
3d5
2p53d6L
XPS
2p53d5
-Q
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 65
3d9L
3d8
NiO: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

2p53d10L
2p53d9
+U-Q  
Charge Transfer Effects
Charge transfer effects

## Slide 66
Tanabe-Sugano with Charge transfer
α 3d8 + β 3d9L
Tanabe-Sugano diagrams with charge transfer
NiO
Cu3+

## Slide 67
=10
NiO
La2Li½Cu½O4
30% 3d8
1A1
30% 3d8
3A2
=-5
=5
=0
=-10
3d8 + 3d9L
Charge Transfer effects
Chem. Phys. Lett. 297, 321 (1998)
Charge transfer effects in XAS

## Slide 68
3d6L
3d5

2p53d7L
2p53d6
+U-Q  
FeIII: Ground state: 3d5 + 3d6L
LMCT and MLCT:  - bonding
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)

## Slide 69
3d4L
3d6L
3d5
FeIII: Ground state: 3d5 + 3d6L + 3d4L

2p53d5L
2p53d7L
2p53d6
+U-Q   - 2

-U+Q   + 2
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 70
FeIII(tacn)2
FeIII(CN)6
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 71
Multiplet calculations
Calculated for an atom/ion
Valence and core spin-orbit coupling
Core and valence electron-electron interaction.
Comparison with experiment
Core hole potential and lifetime
Local symmetry (crystal field)
Spin-spin interactions (molecular field)
Core hole screening effects (charge transfer)
Notes: 71

## Slide 72
First Principle Multiplet calculations
Calculated for an atom/ion
Valence and core spin-orbit coupling
Core and valence electron-electron interaction.
Comparison with experiment
Core hole potential and lifetime
Local symmetry (crystal field)
Spin-spin interactions (molecular field)
Core hole screening effects (charge transfer)
Notes: 72

## Slide 73
2p XAS first-principle codes
SOLIDS
Band structure multiplet (Haverkort, Green, Hariki)
Cluster DFT multiplet (Ikeno, Ramanantoanina, Delley)
MOLECULES
Restricted Active Space CI (Odelius, Kuhn)
Restricted Open-shell CI (Neese)
TDDFT/BSE
Time-Dependent DFT (Joly)
Bethe-Salpeter (Rehr, Shirley)
Multi-channel Multiple-scattering (Kruger)
Notes: 73

## Slide 74
XPS

## Slide 75
I(FIXED)
X-ray absorption and X-ray photoemission
XAS and XPS

## Slide 76
3d6L
Transition metal oxide: Ground state: 3d5 + 3d6L
Energy of 3d6L: Charge transfer energy 
XAS
2p53d7L
+U-Q  

2p53d6
3d5
2p53d6L
XPS
2p53d5
-Q
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 77

+U-Q
Charge Transfer Effects in XAS
Charge transfer effects in XAS

## Slide 78
Charge transfer
Charge transfer effects in XAS
XAS = neutral
Self screened
Small charge transfer satellites

## Slide 79

-Q
Charge Transfer Effects in XPS
Charge transfer effects in XPS

## Slide 80
Charge transfer effects in XPS
Charge transfer effects in XPS
XAS = neutral
Self screened
Small charge transfer satellites
XPS = ionising
Large screening
Large charge transfer satellites

## Slide 81
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 82
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 83
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 84
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 85
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3
LDA + DMFT:
Use actual DMFT-based band structure
result to couple to the localised states
More on Thursday/friday
Phys. Rev. B.100, 075146 (2019)

## Slide 86
Resonant Auger of NiO

## Slide 87
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)

## Slide 88
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)
3d8 → 2p53d9
2p53d9 → 3s03d9ε

## Slide 89
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)
3d8 → 2p53d9
3d9L→ 2p53d10L
2p53d9 → 3s03d9ε
2p53d10L → 3s03d10ε
ONLY 2 PEAKS

## Slide 90
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)

## Slide 91
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)

## Slide 92
Resonant Auger of NiO