## Slide 1
Models Beyond Ligand Field Theory
Quanty Workshop 2019
Robert Green

## Slide 2
Recap: The success of crystal and ligand field theories

## Slide 3
For some material + experiment combinations, LFT is insufficient
1. Perovskite nickelate XAS
2. Rocksalt 3d oxide RIXS
3. Impurity in/on a non-correlated metal

## Slide 4
Case 1: Perovskite Nickelate XAS
Double Clusters for Highly Covalent Oxides

## Slide 5
3d transition metal oxides
Δ
U
U
Δ
PRL 53, 2339 (1985)
J. Phys. F: Metal Phys. 11, 121 (1981)

## Slide 6
Classification of Correlated Compounds
Sawatzky and Green, cond-mat.de/events/correl16/manuscripts/

## Slide 7
Classification of Correlated Compounds
Sawatzky and Green, cond-mat.de/events/correl16/manuscripts/

## Slide 8
Charge Transfer Trends
2+
3+
4+
Mn Fe Co Ni Cu
N | O | F
P | S | Cl
As | Se | Br
Sb | Te | I
+
-
Oxide Trends
Anion Trends
 |  |  | R3+NiO3 | NaCuO2
 | SrFeO3 | SrCoO3 |  | 

## Slide 9
Review of the Perovskite Oxide Crystal Structure
 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | O |  | 
 | Ca | Sc | Ti | V | Cr | Mn | Fe | Co | Ni | Cu |  |  |  |  |  |  | 
 | Sr |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | Ba |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  | La | Ce | Pr | Nd | Pm | Sm | Eu | Gd | Tb | Dy | Ho | Er | Tm | Yb | Lu
Many different combinations of A and B possible

## Slide 10
Perovskite Nickelates: RNiO3
Temperature-dependent metal-insulator transition
“Breathing distortion” in low temperature insulating phase
NdNiO3

## Slide 11
Phase diagram for metal-insulator transition and magnetic order
Perovskite Nickelates: RNiO3

## Slide 12
Thought to be a negative charge transfer system – disobeys formal oxidation state rules
R3+Ni3+(O3)6- → R3+Ni2+(O3)5-
Nickel prefers to be 2+ (3d8 occupation), and there are corresponding “self-doped” holes in oxygen band
MIT can then be understood as “bond disproportionation”:
Perovskite Nickelates: RNiO3
d8L1 (S=1/2) + d8L1 (S=1/2) → d8L0 (S=1) + d8L2 (S=0)

## Slide 13
Experimental absorption and magnetic diffraction data should provide insight on the electron occupation and charge transfer energy
NdNiO3 Experiment
Perovskite Nickelates: RNiO3
One can use creative broadening for d7 LFT to get reasonable XAS, but then the magnetic scattering fails

## Slide 14
Can we improve on ligand field theory? What might be missing?

## Slide 15
Double Cluster Model
Ligand field theory: NiO6 cluster, exact diagonalization
Coulomb
Spin-orbit
Phys. Rev. B 94, 195127 (2016)
Two of these clusters, coupled via symmetric hybridization operator

## Slide 16
Double Cluster Model
Phys. Rev. B 94, 195127 (2016)
and prefactors allow one to gradually turn on coupling between clusters
For perovskite, where two Ni share 1 out of 6 oxygens, we expect
Variations of bond lengths via Harrison’s rules

## Slide 17
Double Cluster Model
Phys. Rev. B 94, 195127 (2016)

## Slide 18
Double Cluster Model
Theory
NdNiO3 Experiment
Phys. Rev. B 94, 195127 (2016)
We can use the model to compute the isotropic and MCD components of the scattering tensor
From these, we can calculate the XAS and magnetic scattering energy dependence, and find excellent agreement with experiment

## Slide 19
Double Cluster Model
The main spectral features are captured by the double cluster model without any breathing distortion
The most important thing is to capture inter-cluster charge fluctuations
Breathing distortion leads to unique spectra at each site, which sum to yield a spectrum exhibiting weak (but important) changes with breathing distortion

## Slide 20
Double Cluster
Single Cluster
Highly Covalent Ground State

## Slide 21
A Note on Complexity
With single cluster ligand field theory, our basis size is
With double cluster ligand field theory, our basis size is
dn | Single | Double
0 | 1.8E+05 | 1.4E+11
1 | 1.7E+05 | 1.1E+11
2 | 1.3E+05 | 6.3E+10
3 | 7.8E+04 | 2.3E+10
4 | 3.9E+04 | 5.6E+09
5 | 1.6E+04 | 8.5E+08
6 | 4.8E+03 | 7.7E+07
7 | 1.1E+03 | 3.8E+06
8 | 1.9E+02 | 9.1E+04
9 | 2.0E+01 | 7.8E+02
10 | 1.0E+00 | 1.0E+00

## Slide 22
Case 2: 2p3d RIXS of Oxides
Impurity models to capture ligand band effects

## Slide 23
Case 2: Anderson Impurity Model for 2p3d RIXS in Oxides
Back to NiO example
During Tuesday tutorial, we saw that ligand field theory gives good agreement with XAS
We added extra broadening in charge transfer region to improve agreement
But for some experiments which directly probe these charge transfer states, we find that ligand field theory fails

## Slide 24
Nickel Oxide 2p3d RIXS
Experimental data from PRL 102, 027401 (2009), courtesy G. Ghiringhelli
Experimental Data
Ligand Field Theory
Ligand field theory is missing the dispersing nature of the charge transfer excitations

## Slide 25
Nickel Oxide 2p3d RIXS
Ligand field theory also shows sharp charge transfer excitations, instead of a band when exciting at resonance
To understand these deficiencies, let’s consider the RIXS process, first from the ligand field theory point of view
[1] PRL 102, 027401 (2009), data courtesy G. Ghiringhelli

## Slide 26
Ligand Field Theory Review
Δ
Δ + U

## Slide 27
XAS
XPS
Δ - Q
Δ + U - Q
Δ + U - Q
Δ + 2U - Q
NiBr2
NiO
Ligand Field Theory Review

## Slide 28
XAS
RIXS
Δ
Δ + U
Ligand Field Theory Review

## Slide 29
Impurity Model
Recall that our ligand states actually form a broad band
So our configurations will have a different energy depending on where the ligand electron came from within the band

## Slide 30
Impurity Model
LFT
Impurity

## Slide 31
RIXS from the Impurity Model Perspective
The dispersing “fluorescence” spectra arise from resonantly exciting different parts of the charge transfer band

## Slide 32
Implementation of impurity model – “Anderson geometry”
...
shell
shells
We “distribute” our total LFT hopping over our set of ligand sites:
The specific and/or set the shape of our band (a.k.a. hybridization function)

## Slide 33
Implementation
In our calculation, we need to include an additional ligand shell (with 10 fermions), for EACH ligand site we want to include (i.e. how finely we want to discretize the band)
Once we have included the shells in Quanty, we simply have to define hopping operators and set onsite energies to form a band
E.g., for a rectangular band of width discretized by points, and total hopping integral ,
...
shell
shells

## Slide 34
A Note on Complexity
With single cluster ligand field theory, our basis size is
With an impurity model having (full) ligand sites, our basis size is
dn | N=1 (LFT) | N=20 | N=100
0 | 1.8E+05 | 3.7E+16 | 2.9E+23
1 | 1.7E+05 | 1.8E+15 | 2.9E+21
2 | 1.3E+05 | 8.2E+13 | 2.6E+19
3 | 7.8E+04 | 3.2E+12 | 2.1E+17
4 | 3.9E+04 | 1.1E+11 | 1.5E+15
5 | 1.6E+04 | 3.2E+09 | 8.7E+12
6 | 4.8E+03 | 7.9E+07 | 4.3E+10
7 | 1.1E+03 | 1.5E+06 | 1.7E+08
8 | 1.9E+02 | 2.2E+04 | 5.1E+05
9 | 2.0E+01 | 2.1E+02 | 1.0E+03
10 | 1.0E+00 | 1.0E+00 | 1.0E+00

## Slide 35
Impurity model RIXS for NiO
Using similar parameters as LFT, but now add a band
Captures both excitations and dispersing charge transfer excitations
XAS
RIXS

## Slide 36
Ghiringhelli et al., JP:CM, 17, 5397 (2005)
Comparison to Experiment
Experiment
Impurity Model

## Slide 37
Improvements in Efficiency
With the Anderson impurity model in the traditional hybridization geometry, the impurity couples directly to each ligand site
The ground state wavefunction then has weight distributed over all ligand sites, leading to a complicated (large) wavefunction
We can transform to a more efficient bath geometry
...
Anderson Geometry
...
Chain Geometry

## Slide 38
Hybridization Operator Layout
Anderson geometry
Chain geometry
Impurity couples to all ligands
Impurity couples to one ligand
Ligands couple to form chain
Examples and comparisons in tutorial session

## Slide 39
Many-body Hamiltonian
Two different basis choices for same 3d impurity Hamiltonian.
Which is better for computing the ground state (iteratively)?

## Slide 40
Case 3: Correlated impurity in/on a non-correlated Metal
Impurity model with metallic bath & natural orbital geometry

## Slide 41
Case 3: Impurity in/on a Metal
From earlier in the week – in spectroscopy we might see bands, excitons, and resonances
Band
Resonance
Exciton
K-edges, DFT
L-edges, MCFT/MLFT/AIM
?

## Slide 42
Case 3: Impurity in/on a Metal
A key property of the oxide impurity model was that the bath of oxygen ligands was completely full (before hybridization)
The oxides are insulators, so any charge fluctuations from the metal to the conduction band are at a higher energy scale and can (usually) be neglected
For an impurity coupled to a metallic bath the problem becomes much more complex (historically called the infrared divergence problem)
...
...
If our starting configuration is , we have many, many low energy configurations of the form which mix into our groundstate.
...

## Slide 43
We can do a bit better by transforming to a full chain + empty chain representation
Case 3: Impurity in/on a Metal
...
...
...
...

## Slide 44
We can do much better by transforming to a natural impurity orbital representation
Case 3: Impurity in/on a Metal
...
...
...
...

## Slide 45
We can do much better by transforming to a natural impurity orbital representation
Case 3: Impurity in/on a Metal
(Nbath=5)
Many-body Hamiltonian

## Slide 46
Energy (eV)
Intensity
W=1
U=20
Q=0.25
Energy (eV)
Intensity
W=1
U=20
Q=0.5
Energy (eV)
Intensity
W=1
U=20
Q=1.0
Energy (eV)
Intensity
W=1
U=20
Q=1.25
Energy (eV)
Intensity
W=1
U=20
Q=1.5
Energy (eV)
Intensity
W=1
U=20
Q=1.75
Energy (eV)
Intensity
W=1
U=20
Q=2.0
Energy (eV)
Intensity
W=1
U=20
Q=0
With our impurity coupled to a metallic bath on a natural impurity orbital basis, we can study band, resonance, and exciton formation in spectra
More details in tutorial session this afternoon
Figure from M. Haverkort