## Slide 1
Resonant Inelastic X-ray Scattering
Resonant X-ray Raman Scattering (RXRS)
Resonant X-ray Emission Spectroscopy (RXES)
Resonant X-ray Energy Loss Spectroscopy (R-XELS)
RIXS

## Slide 2
Ψ0
Core-valence RIXS
2p
electronic
dd, CT
magnon
vibrations

## Slide 3
resonant inelastic x-ray scattering
Notes: 3

## Slide 4
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
3d9
2D
2D5/2
2D3/2
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
ATOMIC

## Slide 5
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
3d9
2D
2D5/2
2D3/2
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
ATOMIC

## Slide 6
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
3d9
2D
2D5/2
2D3/2
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
Only L3 edge
Spin-orbit excitation
Elastic line in 2p3d RIXS
ATOMIC

## Slide 7
Octahedral crystal field splitting
metal ion
in free space
in symmetrical field
t2g
yz xz xy
eg
in octahedral ligand field
x2-y2 z2
x2-y2 yz z2 xz xy
CRYSTAL FIELD EFFECT
3d1
2D
2Eg
2T2g

## Slide 8
Octahedral crystal field splitting
CRYSTAL FIELD EFFECT
3d9
2D
2D5/2
2D3/2
2T2g (1)
2T2g (2)
2Eg

## Slide 9
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
Crystal field excitations
Elastic line in 2p3d RIXS
OCTAHEDRAL
3d9
2D
2D5/2
2D3/2
2T2g (1)
2T2g (2)
2Eg

## Slide 10
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
Crystal field mixes J states
Both L3 and L2 edges
Crystal field excitations
Elastic line in 2p3d RIXS
OCTAHEDRAL
3d9
2D
2D5/2
2D3/2
2T2g (1)
2T2g (2)
2Eg

## Slide 11
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
OCTAHEDRAL
3d9
2D
2D5/2
2D3/2
2T2g (1)
2T2g (2)
2Eg

## Slide 12
Ψ0
Core-core RIXS
2p
electronic
dd, CT
magnon
vibrations
3s

## Slide 13
Resonant Inelastic X-ray Spectroscopy
2p XAS of CaF2
3d0

’
3s13d1
2p53d1
2p3s RIXS of CaF2

## Slide 14
2p3s RIXS of CaF2
Ground state is 3d0
Excitation (i0) 3d0  (x) 2p53d1
Decay (x) 2p53d1  (f) 3s13d1
2p3s RIXS of CaF2

## Slide 15
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d0
1S
1S0
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0

## Slide 16
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d0
1S
1S0
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0

## Slide 17
Octahedral crystal field splitting
metal ion
in free space
in symmetrical field
t2g
yz xz xy
eg
in octahedral ligand field
x2-y2 z2
x2-y2 yz z2 xz xy
CRYSTAL FIELD EFFECT
3d1
2D
2Eg
2T2g

## Slide 18
Atomic Multiplet Theory
CRYSTAL FIELD EFFECT
3dN
J=0
J=4
J=1
J=2
J=3
A1
T2
T1
E
A1
E
T2
A2
T2
T1
T1
    Branching rules:
    Same rules for any quantum number
    S, L or J

## Slide 19
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS

## Slide 20
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS
2 3 7 8 5

## Slide 21
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS
2 3 7 8 5
Dipole selection rule:
ΔJ=T1
(cubic symmetry)

## Slide 22
Atomic Multiplet Theory
X-ray emission from 2p53d1 to 3s13d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3s13d1
1D
3D
1D2
3D1
3D2
T2
E
T2
E
T1
A2
T1
T2
3D3

## Slide 23
Atomic Multiplet Theory
X-ray emission from 2p53d1 to 3s13d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3s13d1
1D
3D
1D2
3D1
3D2
T2
E
T2
E
T1
A2
T1
T2
3D3
Dipole selection rule:
ΔJ=T1 * T1=T1+T2 +E +A1
7x7 matrix

## Slide 24
Phys. Rev. B.
53, 7099 (1996)
Resonant Inelastic X-ray Scattering
3d0

’
3s13d1
2p53d1
2p3s RIXS of CaF2

## Slide 25
Ψ0
1s2p RIXS of transition metal ions
1s
electronic
dd, CT
magnon
vibrations
2p

## Slide 26
CoIII(acac)
K edge and 1s2p RIXS
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
1s2p RIXS of transition metal ions

## Slide 27
CoIII(acac)
K edge and 1s2p RIXS
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
1s2p RIXS of transition metal ions

## Slide 28: Pre-edge and edge
Only quadrupole peaks visible
3d7  1s13d8  2p53d8
CoO
high-spin CoII
3d7 [4T2]
Sharper pre-edge structures in 1s XAS

## Slide 29
Co K edge of LiCoO2
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
K pre-edge of TM oxides (LiCoO2)
Pre-edges structures in 1s XAS

## Slide 30
Co K edge of LiCoO2
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
K pre-edge of TM oxides (LiCoO2)
Pre-edges structures in 1s XAS

## Slide 31
Does HERFD measure X-ray Absorption?
?
?
2p5d dipole
LaF3
2p4f quadrupole
4f0 2p5 4f1

## Slide 32
2p4d RIXS of LaF3
4f0 2p5 4f1  4d9 4f1

## Slide 33
K pre-edge of TM oxides
Pre-edges structures in 1s XAS

## Slide 34
K pre-edge of TM oxides
Pre-edges structures in 1s XAS
J. Phys. Cond. Matt. 21, 104207 (2009); Phys. Rev. B. 81, 115115 (2010)

## Slide 35
RIXS-MCD of CrO2
[Zimmermann et al. J. Elec. Spec (2017)]

## Slide 36
K edge and 1s2p RIXS
Hard x-ray RIXS
Reduce lifetime from 1.5 to 0.2 eV (HERFD XANES)
Reveal new features at pre-edge
Soft x-ray edges with hard x-rays
Spin-polarized XAS
Range extended EXAFS
Background free FY for low conc.
RIXS-MCD

## Slide 37
2p3d RIXS of transition metal ions

## Slide 38
Ψ0
3 2 1 0
2p3d RIXS of transition metal ions
core
electronic
dd, CT
magnon
vibrations

## Slide 39
2p3d RIXS
eV
electron-electron
crystal field
charge transfer
polarization, angles
(in, sample, out)
meV
spin-orbit, magnetic
distortions
vibrations
RIXS 2022: 20 meV
RIXS1998: 500 meV
Notes: 39

## Slide 40
[CoIIW12O40]·
[Van Schooneveld, Hunault et al., unpublished ]
2p3d RIXS of isolated chromium ions (ruby)

## Slide 41
Multiplet challenge: 2p3d RIXS on Cr3+
Notes: 41

## Slide 42
Multiplet challenge: 2p3d RIXS on Cr3+
[Hunault, van Schooneveld, submitted]
Optical resolution can be 0.01 meV
Spin-forbidden dd-excitations limited by experimental resolution
Notes: 42

## Slide 43
Spin-state in LaCoO3 (single crystal)
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 44
Spin state of LaCoO3
E
T2
E
T2
5T2
1A1
E
T2
3T1
NOTE: Term symbols and orbital occupations are only indications: they are mixed by electron-electron, spin-orbit, etc.
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 45
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
dd-excitations + fluorescence
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 46
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
dd-excitations + fluorescence
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 47
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
dd-excitations + fluorescence
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 48
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 49
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
Spin transition is from low-spin to high-spin,
. . . . but is it really high-spin?
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 50
Spin state of LaCoO3
[Sotnikov & KUnes, Sci. Rep 6, 30510 (2016); Wang et al. submitted ]
Order of states at zero Kelvin: LS < HS < IS
Strong coupling between LS and IS (not with HS)
Large dispersion of IS: Excitonic Insulator
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 51
Spin state of LaCoO3
[Wang et al. 2018 ]
q-dep. RIXS
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 52
2p3d RIXS of transition metal ions

## Slide 53
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
3d9
2D
2D5/2
2D3/2
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
Only L3 edge
Spin-orbit excitation
Elastic line in 2p3d RIXS
ATOMIC

## Slide 54
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)

## Slide 55
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)

## Slide 56
Magnon 2p3d RIXS in cuprates

## Slide 57
NiII 3d8 []  2p53d9[jj]  3d8[]
2p3d RIXS of NiO
Notes: Cartoon of a spin-flip transition

## Slide 58
dd
spin-flip
‘spin-flip’
MS
S
2p3d RIXS of NiO
[Phys. Rev. B. 57, 14584 (1998)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 59
2p3d RIXS of NiO
[Phys. Rev. Lett. (2020)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 60
2p3d RIXS of NiO
[Phys. Rev. Lett. (2020)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 61
2p3d RIXS of Fe2O3

## Slide 62
0,1 and 2-magnons in 2p3d RIXS of Fe2O3

## Slide 63
0,1 and 2-magnons in 2p3d RIXS of Fe2O3

## Slide 64
0,1 and 2-magnons in 2p3d RIXS of Fe2O3

## Slide 65
0,1 and 2-magnons in 2p3d RIXS of Fe2O3

## Slide 66
3-magnons in 2p3d RIXS of Fe2O3

## Slide 67
3-magnons in 2p3d RIXS of Fe2O3

## Slide 68
2p3d RIXS
eV
electron-electron
crystal field
charge transfer
polarization, angles
(in, sample, out)
meV
spin-orbit, magnetic
distortions
vibrations
RIXS 2019: 20 meV
RIXS1998: 500 meV
Notes: 68

## Slide 69
Disentangling the A and B sites
2p3d RIXS-MCD
Jeff = 90 meV
[Elnaggar et al. ACS Appl. Mat & Interf. (2019)]
Notes: We first measured XMCD to disentangle the magnetic signals of Fe3O4 as the three Fe ions in Fe3O4
At an incidence energy of 708.8eV (labeled EA), the resonance is dominantly selective to the Fe3+ A sites as concluded by theoretical ligand field multiplet calculations. On the other hand, tuning the incident energy to EB = 709.1 eV excites mainly the Fe3+ B sites.
Measuring the RIXS spectra at the two energies reveal energy loss features centered at ∼ 90 meV for both incident energies
The dichroism sign is reversed between the RIXS measurements at the two energies.
Hence, by measuring Fe 2p3d RIXS at incident energies EA and EB, we can directly probe magnetic exchange of the anti-ferromagnetic Fe A and B sites separately.
We remark that our spin-flip assignment is also consistent with inelastic neutron scattering measurements showing two spin wave modes (∆5 and ∆′2) at ∼ 80meV that nearly do not disperse. These modes were predicted to propagate solely on the Fe B sublattice in agreement with our site selectivity at EB.
Another mode was observed at ∼ 125meV which propagates on the Fe A sublattice and also has a very weak dispersion. We expect to probe this mode by tuning the incident energy to EA, however our current analysis is not enough to establish the displacement of the peak with 35 meV between the two spin-flip excitations.
This methodology could be used for thin films and interfaces to probe selectively specific magnetic species in selective symmetries

## Slide 70
RIXS magnetic angular distribution
Kin
Ein
B
V(0)
H(90)
Fe3+A
[Elnaggar et al. PRM 4, 024415 (2020)/PRL 123, 207210 (2019) / PRB 101, 085107 (2020)
Notes: A complementary measurement to undertake is the spin-flip RIXS-MLD measurement which is sensitive to in-plane moments and site anisotropic effects.
The RIXS magnetic linear angular dependence was measured by rotating the incident polarization (εin) with respect to the crystallographic direction and the external magnetic field.
A strong angular dependence is observed. The angle between εin and the magnetic moment changes as a function of rotation leading to a strong angular dependence at the spin-flip excitation.
The maximum intensity of the spin-flip excitation occurs at ∼ 120◦
Notice that this represents a phase shift between the maximum of the elastic peak intensity and the spin-flip excitation

## Slide 72
Electron yield
Fluorescence Yield (1. dilute limit)
FY (2. state dependent decay)
No XMCD sum rules in FY
FY (3. inverse PFY)
FY (4. dips and peaks)
Yield detection

## Slide 73
X-ray enters sample
Total absorption
Penetration depth λ is inverse proportional to
Yield detection
λ

## Slide 74
Core hole decays by photons (σ) or electrons (σE)
Electrons escape from surface determined by their kinetic energy λ
Electron yield: EY = * σE * λ ~
[Neglect angular dependences]
Electron Yield detection
λ
λ

## Slide 75
Electron Yield detection

## Slide 76
Core hole decays by photons (σ) or electrons (σE)
Photons escape prop. to λ’= ]
Fluorescence yield: FY = * σ * λ
[Neglect angular dependences]
Fluorescence Yield detection
λ

## Slide 77
Fluorescence yield: FY = * σ * λ
= +
λ ~1/
σ is different for edge and background (σB)
Fluorescence Yield detection
ITFY ~

## Slide 78
FY detection of dilute sample
ITFY ~
ITFY ~
ITFY ~

## Slide 79
FY detection of concentrated (bulk) sample
ITFY ~
Non-d
ITFY ~
“saturation & self-absorption”
De-saturation software
(μ(ω) based on CRXO)

## Slide 80
Single synchrotron pulselength is too long
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
XAS of radiation sensitive sample
Notes: 80

## Slide 81
FY-XAS of radiation sensitive sample
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Fluorescence does not measure XAS spectrum
Saturation ?
Notes: 81

## Slide 82
FY-XAS of radiation sensitive sample
Fluorescence does not measure XAS spectrum
NO Saturation
State-dependent decay
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 82

## Slide 83
Yield methods assume a constant ratio between radiative and non-radiative decay
If this ratio is state (= energy) dependent then the related yield methods do not measure XAS.
FY detection: State dependent decay

## Slide 84
FY detection: State dependent decay
FY
EY
L3
L2
Solid State Comm. 92, 991 (1994)

## Slide 85
The dominant yield method is not visibly affected, thus for soft X-rays only FY is affected, not electron yield.
FY detection: State dependent decay

## Slide 86
FY detection (state-dependent, dilute)
ITFY ~
ITFY ~
Main decay of 2p core hole is 2p3d RIXS
Integrate RIXS spectrum to 2p3d PFY
TFY ~ 2p3d PFY
NOTE: “RIXS” has angular dependence effects

## Slide 87
XAS: transmission & FY
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 87

## Slide 88
FY-XAS ≠ XAS L2 edge increases High-energies increase
Fluorescence Yield detection
Kurian J. Phys. Cond. Matt. 24, 435602 (2012)

## Slide 89
XMCD sum rules break down
Ni/Co 20%, Fe 30%, Mn > 100% error
Fluorescence Yield XMCD
Liu, Phys. Rev. B. 96, 054446 (2017)

## Slide 90
ITFY ~ = the integrated RIXS
Measure the partial fluorescence yield of the background.
IBFY ~
1/(1+x) ≈ 1 – x
IBFY ≈ 1 –
Measure a negative XAS spectrum, essentially tracking the probing depth [λ]
FY detection: 3 inverse PFY

## Slide 91
FY detection: 3 inverse PFY
Achkar ea, scientific reports 1, 82 (2011)

## Slide 92
FY detection: 4 dips and peaks
Measure the total fluorescence yield
State-dependent metal PFY + IPFY
ITFY ~
ITFY ~ c1

## Slide 93
FY detection: 4 dips and peaks
Nature Chem. 4, 766 (2012) & Phys. Rev. Letter discussions (2014)