## Slide 1
Introduction to XAS
XAS detection techniques
XAS spectral shape
multiplet calculations
X-ray Absorption Spectroscopy

## Slide 2
Element specific
Sensitive to low concentrations
Applicable under extreme conditions
SPACE: Combination with x-ray microscopy
TIME: femtosecond XAS
RESONANCE: RIXS, RPES, R diffraction
X-ray Absorption Spectroscopy
Notes: XAS is element specific because each element has specific binding energies for its core levels.
The XAS edge energy is essentially given by the core level binding energy.

## Slide 3: Interaction of x-rays with matter
The photon moves towards the atom
Interaction of x-rays with matter

## Slide 4: Interaction of x-rays with matter
The photon is scattered by an electron
Interaction of x-rays with matter
X-ray scattering X-ray diffraction
X-ray scattering is independent of the x-ray energy

## Slide 5: Interaction of x-rays with matter
The photon is scattered by an electron
Interaction of x-rays with matter
X-ray scattering X-ray diffraction

## Slide 6: Interaction of x-rays with matter 1
The photon meets an electron and is annihilated
Interaction of x-rays with matter

## Slide 7: Interaction of x-rays with matter
The electron gains the energy of the photon and is turned into a blue electron.
Interaction of x-rays with matter

## Slide 8: Interaction of x-rays with matter
The blue electron (feeling lonely) leaves the atom
Interaction of x-rays with matter

## Slide 9: Interaction of x-rays with matter
The probability of photon annihilation determines
the intensity of the transmitted photon beam
I0
I (XAS)
Ek (XPS)
Interaction of x-rays with matter

## Slide 10: Interaction of x-rays with matter
XAS, XPS
Elastic scattering (SAXS, XRD)
Inelastic scattering
Mn
X-ray absorption

## Slide 11
Label
Orbital
eV
K
1s
6539
L I
2s
769
L II
2p1/2
650
L III
2p3/2
639
M I
3s
82
M II
3p1/2
47
M III
3p3/2
47
X-ray absorption edges
X-ray Absorption Spectroscopy

## Slide 12
Label
Orbital
eV
K
1s
6539
L I
2s
769
L II
2p1/2
650
L III
2p3/2
639
M I
3s
82
M II
3p1/2
47
M III
3p3/2
47
X-ray absorption edges
X-ray Absorption Spectroscopy
BarKLa
The Nobel Prize in Physics 1917 was awarded to Charles Glover Barkla "for his discovery of the characteristic Röntgen radiation of the elements."

## Slide 13
Label
Orbital
eV
K
1s
6539
L I
2s
769
L II
2p1/2
650
L III
2p3/2
639
M I
3s
82
M II
3p1/2
47
M III
3p3/2
47
X-ray absorption edges
X-ray Absorption Spectroscopy
BarKLa
The Nobel Prize in Physics 1917 was awarded to Charles Glover Barkla "for his discovery of the characteristic Röntgen radiation of the elements."
sharp
principal
diffuse
fundamental
J. Chem. Educ. 84, 757 (2007)

## Slide 14
X-ray Absorption Spectroscopy
Atomic electronic structure X-ray absorption of an atom

## Slide 15
X-ray Absorption Spectroscopy
Atomic electronic structure X-ray absorption of an atom

## Slide 16
X-ray Absorption Spectroscopy
Molecular electronic structure X-ray absorption of a molecule

## Slide 17
4sp
Eg
T2g
O2p
O2s
O 1s ~530 eV
XAS: spectral shape (O 1s)
Electronic structure of a transition metal oxide
Main bonding:
O2p with metal 4sp
Gives valence band and conduction band,
Mixed in character
Additional bonding
O2p with metal 3d;
Gives mixed 3d bands split by crystal field in octahedral symmetry, T2g states have pi-bonding and Eg states have sigma-bonding.
oxygen 1s core state
is localized at an oxygen atom
Notes: 17

## Slide 18
4sp
Eg
T2g
O2p
O2s
O 1s ~530 eV
XAS: spectral shape (O 1s)
transition from oxygen 1s state
to an empty state
oxygen 1s core state
is localized at an oxygen atom
local empty DOS
dipole selection rule:
p-projected DOS
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
[Phys. Rev. B. 40, 5715 (1989); review in Chem. Rev. 120, 4056 (2020)]
Notes: 18

## Slide 19
2p
2s
Phys. Rev. B.40, 5715 (1989)
XAS: spectral shape (O 1s)

## Slide 20
Electronic Structure: TiO2
XAS: spectral shape
E
T2
TiO2: 3d0
E
T2
Cr2O3: 3d0

## Slide 21
Electronic Structure: TiO2
XAS: spectral shape
E
T2
TiO2: 3d0
E
T2
Cr2O3: 3d0
4 >6
6
2 >3
5 >6

## Slide 22
Electronic Structure: TiO2
XAS: spectral shape
E
T2
Fe2O3: 3d5
E
T2
NiO: 3d8

## Slide 23
Electronic Structure: TiO2
XAS: spectral shape
Fe2O3: 3d5
E
T2
NiO: 3d8
E
T2
2 >3
3
2 >3
0
0

## Slide 24
Phys. Rev. B.40, 5715 (1989); 48, 2074 (1993)
XAS: spectral shape (O 1s)
oxygen 1s > p DOS

## Slide 25
Final State Rule: Spectral shape of XAS looks like final state DOS
TiSi2
Phys. Rev. B. 41, 11899 (1991)
XAS: spectral shape

## Slide 26
XAS codes:
Multiple scattering: FEFF, FDMNES, etc.
Band structure: WIEN2K, Quantumespresso, etc.
Real-space DFT: ADF, ORCA, etc.
TiSi2
Phys. Rev. B. 41, 11899 (1991)
XAS: spectral shape

## Slide 27
XAS: spectral shape (O 1s)
Crystal structure
Electronic structure calculation, for example Density Functional Theory (DFT)
(in the presence of the core hole)
Calculation of the oxygen
p-projected local empty DOS
Compare with experiment
CODES: FEFF, Wien2K, VASP, QE, etc.

## Slide 28
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
XAS: spectral shape (Ti 2p)
Expect the d (and s-) projected Ti DOS
Why is experiment different?
2p > 3d
Notes: 28

## Slide 29
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
XAS: spectral shape (Ti 2p)
Expect the d (and s-) projected Ti DOS
2p spin-orbit coupling (~6 eV)
2p > 3d
Notes: 29

## Slide 30
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
XAS: spectral shape (Ti 2p)
Expect local d-projected Ti DOS
Core spin-orbit splitting
Overlap of core 2p and valence 3d states
>> many electron excitations dominate
2p3d 2-electron integrals
Notes: 30

## Slide 31
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
IXAS = |< 2p5 3d1 |dipole| 3d0>|2 [E=0]
Single electron (excitation) approximation breaks down :
IXAS = |<3d |dipole| 2p>|2 
X-ray absorption
XAS: spectral shape (Ti 2p)
Can NOT approximate 2p-3d interaction as extra potential
Large core hole spin-orbit coupling

## Slide 32
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
IXAS = |< 1s1 2p5 |dipole| 2p4>|2 [E=0]
Single electron (excitation) approximation :
IXAS = |<2p |dipole| 1s>|2 
X-ray absorption
XAS: spectral shape (O 1s)
Can neglect local 2p-2p interaction
Can approximate 1s-2p interaction as extra potential
No core hole spin-orbit coupling

## Slide 33: XAS
Single Particle:
1s edges
(DFT codes, TD-DFT)
Total energy:
2p, 3s, 3p edges
(Multiplet codes)
XAS: two models

## Slide 34
X-ray absorption & Auger
Decay of 3d/valence electron to 3p core state
Energy used to excite a 3d/valence electron
Auger electron spectroscopy
X-ray Absorption Spectroscopy
Notes: 34

## Slide 35
X-ray Absorption Spectroscopy
1s core state
Notes: 35

## Slide 36
XAS: detection techniques

## Slide 37
Use decay channels as detector
XAS: detection techniques
Uniform thickness
Uniform concentration of absorbing element
Thin enough for photons

## Slide 38
X-ray penetration lengths &
electron escape depths
100-1000 nm
(CXRO, but 20 nm for L edges)
1-5 nm
XAS: detection techniques

## Slide 39
Use decay channels as detector
XAS: detection techniques
X-ray penetrate 1000 nm (λX)
Electrons escape from 5 nm (λE)
Number of core holes created in first 5 nm is proportional to μ
ITEY ~ 1 / λX = μX

## Slide 40
Transmission
(pinhole, saturation > thin samples)
Electron Yield
(surface sensitive)
Fluorescence Yield
(saturation & self-absorption:
> dilute samples)
[L edges are intrinsically distorted]
XAS: detection techniques

## Slide 41
Interpretation of spectral shapes
XAS: spectral shape
Notes: 41

## Slide 42: XAS
Single Particle:
1s edges
(DFT codes, TD-DFT)
Total energy:
2p, 3s, 3p edges
(Multiplet codes)
XAS: two models

## Slide 43
Charge Transfer Multiplet program
Used for the analysis of XAS, EELS,
Photoemission, Auger, XES involving d and f-shells
ATOMIC PHYSICS

GROUP THEORY

MODEL HAMILTONIANS
CHARGE TRANSFER MULTIPLETS
Notes: The TT-multiplets program can be used to explain the spectral shapes of all core level spectroscopies. XAFS, photoemission, auger, etc.
The program combines three advanced computer codes, an atomic physics code to describe all atomic interactions, a group theory code to describe the local symmetry (think of crystal fields) and model Hamiltonians to describe many body effects correlated systems.
AS A SIDE REMARK I WOULD LIKE TO MENTION that the active site in a catalyst is a perfect example of a correlated system. (in biocatalysis this is often realised)
The integrated program gives accurate descriptions of core level spectra, from a set of uniform electronic structure parameters.
The program is important for all of the new spectroscopies that I will describe.
The program is distributed from my homepage and it is used at some 50 institutes worldwide.

## Slide 44
Atomic Multiplet Theory
=E
Kinetic Energy
Nuclear Energy
Electron-electron interaction
Spin-orbit coupling
ATOMIC MULTIPLETS

## Slide 45
Atomic Multiplet Theory
X X
=E
Kinetic Energy
Nuclear Energy
Electron-electron interaction
Spin-orbit coupling
ATOMIC MULTIPLETS

## Slide 46
Spin-orbit coupling

## Slide 47
Term Symbols
Spin-orbit coupling
H 2p orbital 0.00004 eV
Na 3p orbital 0.002 eV
Room temperature 0.025 eV
Ni 3d orbital 0.05 eV
Gd 4f orbital 0.2 eV
Shallow core hole
Ni 2p orbital 10 eV
Deep core hole
Pt 2p orbital 2000 eV

## Slide 48
2S+1LJ
Term Symbol
Term symbols

## Slide 49
Term symbols of a 2p13d1 configuration
2p1  2P1/2, 2P3/2 (S=1/2, L=1)
3d1  2D3/2, 2D5/2 (S=1/2, L=2)
Term Symbols
Term symbols

## Slide 50
Term symbols of a 2p13d1 configuration
2p1  2P1/2, 2P3/2 (S=1/2, L=1)
3d1  2D3/2, 2D5/2 (S=1/2, L=2)
2p13d1
 Smax = S1 + S2 = 1
 Smin = |S1 - S2| = 0
 Lmax = S1 + S2 = 3
 Lmin = |S1 - S2| = 1
 S and L: steps of 1
 S = {0,1}; L = {1,2,3}
Term Symbols
Term symbols

## Slide 51
Term symbols of a 2p13d1 configuration
2p13d1
 S = {0,1}; L = {1,2,3}
 1P
 1D
 1F
 3P
 3D
 3F
Term Symbols
Term symbols

## Slide 52
Term symbols of a 2p13d1 configuration
2p13d1
 S = {0,1}; L = {1,2,3}
 1P1
 1D2
 1F3
 3P012
 3D123
 3F234
Term Symbols
Term symbols

## Slide 53
2p XAS of TiO2
2p XAS of Ti4+ ions
Ground state of Ti4+ is 3d0
Dipole transition 3d02p53d1
Ground state symmetry: 1S0
Final state symmetry: 2P2D gives
1P, 1D, 1F, and 3P, 3D, 3F
Atomic multiplets: 2p XAS of Ti4+

## Slide 55
3d0 XAS calculation
Spin-orbit = 4.0 eV
Electron-electron = 5.0 eV
Spin-orbit = 0.4 eV
Electron-electron = 9 eV
Atomic multiplets: 2p XAS of Ti4+

## Slide 56
Term Symbols and XAS
    TiIV ion in TiO2:
    Ground state: 3d0
    Final state: 2p53d1
    Dipole transition: p-symmetry
    3d0-configuration: 1S, 2p13d9-configuration: 2P2D = 1,3PDF
    ,
Atomic multiplets: 2p XAS of Ti4+

## Slide 57
Term Symbols and XAS
    TiIV ion in TiO2:
    Ground state: 3d0
    Final state: 2p53d1
    Dipole transition: p-symmetry
    3d0-configuration: 1S, 2p13d9-configuration: 2P2D = 1,3PDF
    transition: 1S 1P = 1P
    possible final states: 1P ,
Atomic multiplets: 2p XAS of Ti4+

## Slide 58
Term Symbols and XAS
    TiIV ion in TiO2:
    Ground state: 3d0
    Final state: 2p53d1
    Dipole transition: p-symmetry
    3d0-configuration: 1S, j=0 2p13d9-configuration: 2P2D = 1,3PDF j’=0,1,2,3,4
    p-transition: 1P j=+1,0,-1
    ground state symmetry: 1S0
    possible final states: 1P1,3P1,3D1,
Atomic multiplets: 2p XAS of Ti4+

## Slide 59
ATOMIC MULTIPLETS 3d1
5 orbitals (each spin-up or spin-down) >> total 10 states
No electron-electron interaction: all states have the same energy
Quantum numbers: L=2 and S=½, notation as term symbol: 2S+1L= 2D

## Slide 60
ATOMIC MULTIPLETS 3d1
Spin-orbit coupling couples L and S quantum numbers to a total quantum number J
Jmax= L+S = 5/2, Jmin= |L-S|= 3/2, Integer steps of J.
Two term symbols: L=2, S=½, and J = 5/2 >> notation as term symbol: 2S+1LJ= 2D5/2
L=2, S=½, and J = 3/2 >> notation as term symbol: 2S+1LJ= 2D3/2

## Slide 61
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d1
3d1
2D
2D3/2
2D5/2
electron-electron
interaction
spin-orbit
coupling
(~50 meV)

## Slide 62
ATOMIC MULTIPLETS 3d2
5 spin-up orbitals give 4 + 3 + 2 + 1 = 10 paired 3d2 states
5 spin-down orbitals give 10 paired down-down 3d2 states
There are 5x5 = 25 up-down states
In total 10+10+25 = 45 states
Can also be calculated as 10 x 9 / 2 = 45 states
Electron-electron interaction is different for different orbital combinations
There will be a number of different states with different energies.
Analysis shows that the states are 1S, 3P, 1D, 3F and 1G

## Slide 63
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d2
3d2
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
electron-electron
Interaction
(~2 eV)
spin-orbit
coupling
(~50 meV)
    Ground state:
    Given by Hunds rules
    max S
    max L
    min J (if less than half full)

## Slide 64
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d8
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
electron-electron
Interaction
(~2 eV)
spin-orbit
coupling
(~50 meV)
    Ground state:
    Given by Hunds rules
    max S
    max L
    max J (if more than half full)

## Slide 65
Atomic Multiplet Theory
X-ray absorption from 3d8 to 2p53d9
2p53d9
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
Dipole selection rule:
ΔJ=-1, 0 or +1

## Slide 66
Atomic Multiplet Theory
X-ray absorption from 3d8 to 2p53d9
2p53d9
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
Dipole selection rule:
ΔJ=-1, 0 or +1

## Slide 67
Atomic multiplets
2p XAS of NiO with atomic multiplets

## Slide 68
t2g states
Crystal Field Effects
eg states
crystal field effect