## Slide 1
Charge Transfer Multiplet program
Used for the analysis of all core level spectroscopies involving d and f-shells
Write down all core level spectroscopies
Excitation
Decay
Resonances/scattering
CHARGE TRANSFER MULTIPLETS
Notes: The TT-multiplets program can be used to explain the spectral shapes of all core level spectroscopies. XAFS, photoemission, auger, etc.
The program combines three advanced computer codes, an atomic physics code to describe all atomic interactions, a group theory code to describe the local symmetry (think of crystal fields) and model Hamiltonians to describe many body effects correlated systems.
AS A SIDE REMARK I WOULD LIKE TO MENTION that the active site in a catalyst is a perfect example of a correlated system. (in biocatalysis this is often realised)
The integrated program gives accurate descriptions of core level spectra, from a set of uniform electronic structure parameters.
The program is important for all of the new spectroscopies that I will describe.
The program is distributed from my homepage and it is used at some 50 institutes worldwide.

## Slide 2
3d8 + ω
2p53d9
2p53d8+e’
XAS
XPS
X-ray spectroscopies

## Slide 3
3d8 + ω
2p53d9
2p53d8+e’
XAS
XPS
XES
RIXS
3d8 + ω’
X-ray spectroscopies

## Slide 4
3d8 + ω
2p53d9
2p53d8+e’
XAS
XPS
3p43d9+e’
XES
RIXS
AES
3d8 + ω’
RAES
X-ray spectroscopies

## Slide 5
3d8 + ω
2p53d9
2p53d8+e’
3d7 + e’
XAS
XPS
3p43d9+e’
XES
RIXS
AES
3d8 + ω’
RAES
RPES
X-ray spectroscopies

## Slide 6
3d8 + ω
2p53d9
2p53d8+e’
3d7 + e’
XAS
XPS
3p43d9+e’
XES
RIXS
AES
3d8 + ω’
RAES
RPES
XES
XES
3d7 +e’+ω’
X-ray spectroscopies

## Slide 7
3d8 + ω
2p53d9
2p53d8+e’
3d7 + e’
XAS1
XPS2
3p43d9+e’
XES3
RIXS5
AES4
3d8 + ω’
RAES6
RPES7
XES
XES
3d7 +e’+ω’
X-ray spectroscopies
IXS8

## Slide 8
3d8 + e
2p53d10
APS
Electron spectroscopies

## Slide 9
3d8 + e
2p53d10
APS
Electron spectroscopies
XES
RIPES
3d9 + ω’

## Slide 10
3d8 + e
2p53d10
APS
Electron spectroscopies
XES
RIPES
3d9 + ω’
3d8+e’
AES
REELS

## Slide 11
3d8 + e
2p53d10
APS9
Electron spectroscopies
XES
RIPES10
3d9 + ω’
3d8+e’
AES
REELS11
EELS12
RIXS
RAES
RPES
XES
RIPES
REELS

## Slide 12
Resonant spectroscopies
RIXS (ω,ω’)
RAES
RPES
XES
RIPES
REELS
(+ coincidences) (+ polarizations) (+ momentum)
(+ time, space)
X-ray in (ω)
X-ray out (ω’)
RIXS

## Slide 13
Resonant spectroscopies
RIXS (ω,ω’)
RAES (ω,e’)
RPES
XES
RIPES
REELS
(+ coincidences) (+ polarizations) (+ momentum)
(+ time, space)
X-ray in (ω)
Electron out (e’)
RAES

## Slide 14
Resonant spectroscopies
RIXS (ω,ω’)
RAES (ω,e’)
RPES (ω,e’)
XES (ω’,e’)
RIPES
REELS
(+ coincidences) (+ polarizations) (+ momentum)
(+ time, space)
X-ray out (ω’)
Electron out (e’)
XES

## Slide 15
Resonant spectroscopies
RIXS (ω,ω’)
RAES (ω,e’)
RPES (ω,e’)
XES (ω’,e’)
RIPES (e,ω’)
REELS (e,e’)
(+ coincidences) (+ polarizations) (+ momentum)
(+ time, space)
X-ray out (ω’)
Electron out (e’)
XES

## Slide 16
Charge Transfer Multiplet program
Used for the analysis of XAS, EELS,
Photoemission, Auger, XES involving d and f-shells
ATOMIC PHYSICS

GROUP THEORY

MODEL HAMILTONIANS
CHARGE TRANSFER MULTIPLETS
Notes: The TT-multiplets program can be used to explain the spectral shapes of all core level spectroscopies. XAFS, photoemission, auger, etc.
The program combines three advanced computer codes, an atomic physics code to describe all atomic interactions, a group theory code to describe the local symmetry (think of crystal fields) and model Hamiltonians to describe many body effects correlated systems.
AS A SIDE REMARK I WOULD LIKE TO MENTION that the active site in a catalyst is a perfect example of a correlated system. (in biocatalysis this is often realised)
The integrated program gives accurate descriptions of core level spectra, from a set of uniform electronic structure parameters.
The program is important for all of the new spectroscopies that I will describe.
The program is distributed from my homepage and it is used at some 50 institutes worldwide.

## Slide 17
3d XAS of rare earths
4f electrons are localized
No effect of surroundings (crystal field < lifetime broadening)
3d XAS is self screened > no charge transfer effect
Initial state
electron-electron interaction.
Valence spin-orbit coupling
Final state
+ core hole – valence hole ‘multiplet’ interaction.
+ core hole spin-orbit coupling

## Slide 18
3d XAS of rare earths
Nd3+ 4f3 system: ground state is 4I9/2

## Slide 19
2p XAS of 3d transition metal oxides
3d electrons are less localized
Effect of surroundings (crystal field effect)
3d XAS is self screened > weak charge transfer effect
Initial state
electron-electron interaction.
valence spin-orbit coupling
crystal field effect
Final state
core hole – valence hole ‘multiplet’ interaction.
core hole spin-orbit coupling
crystal field effect

## Slide 20
t2g states
Crystal Field Effects
eg states
crystal field effect

## Slide 21
Comparison with Experiment
2p XAS of ScF3 with crystal field multiplets
PHYS. Rev. B. 41, 928 (1990)

## Slide 22
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d0
1S
1S0
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0

## Slide 23
Octahedral crystal field splitting
metal ion
in free space
in symmetrical field
t2g
yz xz xy
eg
in octahedral ligand field
x2-y2 z2
x2-y2 yz z2 xz xy
CRYSTAL FIELD EFFECT
3d1
2D
2Eg
2T2g

## Slide 24
Atomic Multiplet Theory
CRYSTAL FIELD EFFECT
3dN
J=0
J=4
J=1
J=2
J=3
A1
T2
T1
E
A1
E
T2
A2
T2
T1
T1
    Branching rules:
    Same rules for any quantum number
    S, L or J

## Slide 25
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS

## Slide 26
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS
2 3 7 8 5

## Slide 27
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS
2 3 7 8 5
Dipole selection rule:
ΔJ=T1
(cubic symmetry)

## Slide 28
Comparison with Experiment
2p XAS of ScF3 with crystal field multiplets
PHYS. Rev. B. 41, 928 (1990)

## Slide 29
valence e-e interactions Fdd
core-valence e-e Fpd Gpd
core & valence spin-orbit ζ
crystal field 10Dq, Ds, Dt
molecular field, M or H
e-e screening κ
charge transfer Δ, U, Q
hopping TΓ
ionic 3d
(4d, 5d)
4f, 5f
covalent 3d
mixed valence f
ATOMIC
SYMMETRY
BONDING
Multiplet calculations

## Slide 30
valence e-e interactions Fdd
core-valence e-e Fpd Gpd
core & valence spin-orbit ζ
crystal field 10Dq, Ds, Dt
molecular field, M or H
e-e screening κ
charge transfer Δ, U, Q
hopping TΓ
ionic 3d
(4d, 5d)
4f, 5f
3d ions
covalent 3d
mixed valence f
ATOMIC
SYMMETRY
BONDING
Multiplet calculations

## Slide 31
Hubbard U for a 3d8 ground state:
U= E(3d7) + E(3d9) – E(3d8) – E(3d8)
Ligand-to-Metal Charge Transfer (LMCT):
= E(3d9L) – E(3d8)
Charge Transfer Effects
Charge transfer effects

## Slide 32
Charge Transfer Effects
Main screening mechanism in XAS of oxides:
Ligand-to-metal charge transfer
Charge transfer energy  is important for XAS
Hubbard U is NOT important for XAS spectral shape (It is important for (e.g.) XPS spectral shapes)
Charge transfer effects

## Slide 33
3d9L
Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

3d8
Ground State
Charge transfer effects in XAS and XPS
transition metal oxides

## Slide 34

Charge Transfer Effects
3d8
3d9L

## Slide 35

Charge Transfer Effects
3d8
3d9L
9
8

## Slide 36
β 3d8 - α 3d9L
α 3d8 + β 3d9L

Charge Transfer Effects
3d8
3d9L

## Slide 37
3d9L
3d8
NiO: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

2p53d10L
2p53d9
+U-Q  
Charge Transfer Effects
Charge transfer effects

## Slide 38
β 3d8 - α 3d9L
α 3d8 + β 3d9L

+U-Q  
β’ c3d9 – α’ c3d10L
α' c3d9 + β’ c3d10L
~0
~1
Intensity bonding combination: [α α’+ β β’]2
α  α’  (α2+ β2)2 =1
Charge transfer effects

## Slide 39
β 3d5 - α 3d6L
α 3d5 + β 3d6L

+U-Q  
β’ c3d6 – α’ c3d7L
α' c3d6 + β’ c3d7L
~0
~1
Intensity anti-bonding combination: [α β’- β α’]2
α  α’  (αβ – βα)2 =0
Charge transfer effects

## Slide 40
Neutral experiments are self-screened
XAS, optical, EPR, EELS, RIXS
>> small screening satellites
>> crystal field theory can be used
Ionising experiments are not self-screened
XPS, Auger,
>> large screening > large satellites
>> crystal field theory can not be used
Charge Transfer Effects
Charge transfer effects

## Slide 41
3d6L
Transition metal oxide: Ground state: 3d5 + 3d6L
Energy of 3d6L: Charge transfer energy 
XAS
2p53d7L
+U-Q  

2p53d6
3d5
2p53d6L
XPS
2p53d5
-Q
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 42
3d9L
3d8
NiO: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

2p53d10L
2p53d9
+U-Q  
Charge Transfer Effects
Charge transfer effects

## Slide 43
Tanabe-Sugano with Charge transfer
α 3d8 + β 3d9L
Tanabe-Sugano diagrams with charge transfer
NiO
Cu3+

## Slide 44
=10
NiO
La2Li½Cu½O4
30% 3d8
1A1
30% 3d8
3A2
=-5
=5
=0
=-10
3d8 + 3d9L
Charge Transfer effects
Chem. Phys. Lett. 297, 321 (1998)
Charge transfer effects in XAS

## Slide 45
3d6L
3d5

2p53d7L
2p53d6
+U-Q  
FeIII: Ground state: 3d5 + 3d6L
LMCT and MLCT:  - bonding
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)

## Slide 46
3d4L
3d6L
3d5
FeIII: Ground state: 3d5 + 3d6L + 3d4L

2p53d5L
2p53d7L
2p53d6
+U-Q   - 2

-U+Q   + 2
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 47
FeIII(tacn)2
FeIII(CN)6
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 48
Multiplet calculations
Calculated for an atom/ion
Valence and core spin-orbit coupling
Core and valence electron-electron interaction.
Comparison with experiment
Core hole potential and lifetime
Local symmetry (crystal field)
Spin-spin interactions (molecular field)
Core hole screening effects (charge transfer)
Notes: 48

## Slide 49
First Principle Multiplet calculations
Calculated for an atom/ion
Valence and core spin-orbit coupling
Core and valence electron-electron interaction.
Comparison with experiment
Core hole potential and lifetime
Local symmetry (crystal field)
Spin-spin interactions (molecular field)
Core hole screening effects (charge transfer)
Notes: 49

## Slide 50
2p XAS first-principle codes
SOLIDS
Band structure multiplet (Haverkort, Green, Hariki)
Cluster DFT multiplet (Ikeno, Ramanantoanina, Delley)
MOLECULES
Restricted Active Space CI (Odelius, Kuhn)
Restricted Open-shell CI (Neese)
TDDFT/BSE
Time-Dependent DFT (Joly)
Bethe-Salpeter (Rehr, Shirley)
Multi-channel Multiple-scattering (Kruger)
Notes: 50

## Slide 51
XPS

## Slide 52
I(FIXED)
X-ray absorption and X-ray photoemission
XAS and XPS

## Slide 53
3d6L
Transition metal oxide: Ground state: 3d5 + 3d6L
Energy of 3d6L: Charge transfer energy 
XAS
2p53d7L
+U-Q  

2p53d6
3d5
2p53d6L
XPS
2p53d5
-Q
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 54
Charge transfer
Charge transfer effects in XAS
XAS = neutral
Self screened
Small charge transfer satellites

## Slide 55

+U-Q
Charge Transfer Effects in XAS
Charge transfer effects in XAS

## Slide 56

-Q
Charge Transfer Effects in XPS
Charge transfer effects in XPS

## Slide 57
Charge transfer effects in XPS
Charge transfer effects in XPS
XAS = neutral
Self screened
Small charge transfer satellites
XPS = ionising
Large screening
Large charge transfer satellites

## Slide 58
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 59
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 60
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 61
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 62
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3
LDA + DMFT:
Use actual DMFT-based band structure
result to couple to the localised states
More on Thursday/friday
Phys. Rev. B.100, 075146 (2019)

## Slide 63
Resonant Auger of NiO

## Slide 64
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)

## Slide 65
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)
3d8 → 2p53d9
2p53d9 → 3s03d9ε

## Slide 66
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)
3d8 → 2p53d9
3d9L→ 2p53d10L
2p53d9 → 3s03d9ε
2p53d10L → 3s03d10ε
ONLY 2 PEAKS

## Slide 67
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)

## Slide 68
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)

## Slide 69
Resonant Auger of NiO