## Slide 1
DFT calculation of electronic structure: an introduction
Application to K-edge XAS
Amélie Juhin
Sorbonne Université-CNRS (Paris)

## Slide 2
probe of structural and electronic properties of materials
local probe: up to 5-10 Å around the absorbing element
polarized spectra (XNLD)
isotropic spectra
isotropic spectra
1 eV shift
coordination number fingerprint
tremendous amount of information
needs for calculations
About XANES spectroscopy at the K-edge

## Slide 3
probe of structural and electronic properties of materials
K edge: 1s p transitions (mainly)
tremendous amount of information with variable core-hole effects
selection rules
selective probe of empty states localized on the absorber
isotropic spectra
isotropic spectra
polarized spectra (XNLD)
About XANES spectroscopy at the K-edge

## Slide 4
Basic issue: calculation of the absorption cross section
for a material, i.e., a system of N electrons + Nat nuclei
incident x-ray energy
operator of
the interaction between
x-rays and the system
initial state:
ground state of the system
with energy , degenerescence
final state:
excited state of the system
of energy .
XANES modeling
strong e-- e- interaction
multielectronic approach
ex : L2,3 edges of 3d elements
weak e- - e- interaction
monoelectronic approach (Density Functional Theory)
ex : K edges

## Slide 5
Part 1
Introduction to electronic structure calculation using DFT

## Slide 6
Basic issue
Nat atom system :
N electrons, mass m, charge q < 0, position ri (i = 1, …, N)
Nat nuclei, mass MI, charge qI , position RI (I = 1, …, Nat)
+

## Slide 7
Born-Oppenheimer approximation
The nuclear motion is much slower than the electronic motion  separation
The nuclei are considered at fixed positions in the electronic motion study
Positions RI  parameter
m < MI
(m / mproton ≈ 1836)
Order of magnitude of the velocity ratio
Electron :
≈ 10 eV
Nucleus :
≈ 10 meV
≈ 103

## Slide 8
Born-Oppenheimer approximation
Electronic Hamiltonian
parameter
constant

## Slide 9
Multielectronic Schrödinger equation
antisymmetric (electrons are fermions)

## Slide 10
with
spinorbital
We can solve it for a system of non-interacting electrons !
solution
: Slater determinant (SD) - 1929
build from N spinorbital functions
Multielectronic Schrödinger equation

## Slide 11
Slater Determinant
Properties :
  antisymmetric
  Pauli exclusion principle satisfied
Ground state

## Slide 12
solution
: Linear combination of an infinite number of Slater determinants
configuration interaction (“brute force”)
Multielectronic Schrödinger equation
αmax= 10  252 SD
αmax= 20  15, 504 SD
αmax= 50  2, 118, 760 SD
N = 20 αmax= 30  3, 004, 015 SD
N = 5

## Slide 13
Mean-field approximation
Non-interacting electrons
Exact solution : SD
Interacting electrons
Exact solution : ∞ LC of SD
Mean-field approximation
Approximative solutions
Exact multilelectronic Hamiltonian
Effective multielectronic Hamiltonian : mean-field Hamiltonian
with
Solutions :
Slater
determinants

## Slide 14
Monoelectronic Schrödinger solved self-consistently (SCF)
with
electron density
Mean-field approximation

## Slide 15
Mean-field methods: examples
Hartree (H)
Hartree-Fock (HF)
Density Functional Theory (DFT)

## Slide 16
Hartree (H) - 1927
Coulomb interaction between one electron and the electron density
Hartree multielectronic
wave function
product of monoelectronic wave functions
=
Pauli exclusion principle
exchange not taken into account
includes a self-interaction term (if i = j)

## Slide 17
Hartree-Fock (HF) - 1935
exchange included:
the multielectronic wave function as a (unique) SD
additional term that depends on the spin state and the antisymmetric character of the SD :
strictly compensates the self-interaction term when electrons i and j have the same spin state
BUT no correlation between electrons with opposite spins
Correlation energy:
difference between the exact total energy of N-electrons system and the total energy obtained using HF

## Slide 18
Density functional theory (DFT): definition
exact theory
for systems of N interacting electrons
within an external potential

## Slide 19
DFT: Hohenberg and Kohn theorems (1964)
The (non-degenerate) ground state electron density uniquely determines (to a constant)
the external potential (and thus all the properties of the system).
There is a universal density functional , not depending explicitly on , defined as :
with
basic variable

## Slide 20
DFT: Hohenberg and Kohn (1964)
Total energy
E[]

Egs
gs
Variational principle
Exact theory but
question 1

## Slide 21
DFT: Kohn and Sham (1965)
also valid for N non-interacting electrons (Ve-e= 0)
Hohenberg - Kohn theorems valid
for any N-electrons system
Kohn – Sham ansatz
We can find an external potential VKS(r)
for a fictitious system of non-interacting electrons,
giving the same ground state electron density
as the real system
Exact theory BUT
question 2

## Slide 22
DFT: Kohn and Sham (1965)
system of N non-interacting electrons, in an external potential VKS(r),
which gives the same gs electron density as the real system
Kohn-Sham fictitious
system:
Ground state : SD build from N orbitals (monoelectronic)
Kohn-Sham orbitals solutions of:
Kinetic energy of the fictitious system
(indice s : « single particle »)
electron density
(1)

## Slide 23
DFT: Kohn and Sham (1965)
Hartree energy:
What we can write as a functional of the electron density in Ve-e :
we partially answered question 1 !
exchange and correlation energy

## Slide 24
DFT: Kohn and Sham (1965)
Total energy
minimization
Ground state total energy
variational principle applied to E[ρ] with respect to KS orbitals with the constraint:
(2)
exchange and correlation potential

## Slide 25
DFT: Kohn and Sham (1965)
Kohn-Sham equations
Schrödinger equations of the fictitious system
Kohn – Sham potential
We partially answered question 2 !
(2)
(1)

## Slide 26
DFT: Kohn and Sham (1965)
Exact theory:
A Vxc potential that compensates the approximations
introduced by the mean-field approaches
necessarily exist !
ground state : self-consistent field (SCF) resolution of the Kohn – Sham equations
different forms of exchange-correlation functionals
DFT exact theory
useless
approximate theory widely used
In practice:

## Slide 27
DFT: exchange and correlation functionals
In the LDA, DFT is still exact for an homogeneous electron gas.
The Local Density Approximation (LDA)
the simplest
exchange - correlation energy for a particle in a homogeneous electron gas (with density ρ)
known analytically
(Dirac exchange energy)
calculated
using Ceperley-Alder Monte-Carlo method,
or other parametrization (ex: Hedin-Lundqvist)

## Slide 28
Generalized Gardient Approximation (GGA)
the density gradient at r is taken into account
Various parameterizations
example: the PBE functional
J.P. Perdew, K. Burke & M. Ernzerhof « Generalized Gradient Approximation Made Simple » Phys. Rev. Lett., 77:3865‎ (1996).
DFT: exchange and correlation functionals

## Slide 29
Hybrid functionals (H-GGA)
combine the exchange and the correlation obtained by using GGA methods with a given proportion of the exchange described by Hartree-Fock
The most used: B3LYP
(Becke - 3 parameters - Lee, Yang, Parr)
DFT: exchange and correlation functionals

## Slide 30
DFT: SCF cycle
Crystal structure
atomic calculation
 atomic r
Superimposition of atomic r
r crystal= r in
1st step

## Slide 31
DFT: SCF cycle
Potential calculation
Poisson equation
KS orbitals calculation
Kohn and Sham equations
Calculation of  out(r)
in(r)
Convergence?
YES
STOP
NO
mixing
 in(r) &  out(r)

## Slide 32
ParaGauss
PARATEC
PARSEC
PC GAMESS
PLATO
Parallel Quantum Solutions
PWscf (Quantum Espresso)
Q-Chem
SIESTA
Socorro
Spartan
SPR-KKR
TURBOMOLE
VASP
WIEN2k
Abinit
ADF
AIMPRO
Augmented Spherical Wave
Atomistix Toolkit
CADPAC
CASTEP
CP2K
CPMD
CRYSTAL
DACAPO
DALTON
deMon2K
DFT++
DMol3
EXCITING
Fireball
FLEUR
GAMESS (UK)
GAMESS (US)
GAUSSIAN
GPAW
JAGUAR
MOLCAS
MOLPRO
MPQC
NWChem
OpenMX
ORCA
Solid state physics and quantum chemistry
non-exhaustive list
DFT: softwares

## Slide 33
DFT: softwares
infinite
number
of atoms
real space
cluster
no periodicity constraint (amorphous and crystalline materials)
suited to molecules
1st Brillouin zone
periodic boundary conditions
or
suited to cristals supercell
the main differences between them

## Slide 34
Basis to expand the Kohn-Sham orbitals
Atomic orbitals
Gaussians
LCAO
Muffin-tin orbitals
spherical waves
LMTO,multiple scattering
Plane waves
Pseudopotentials
atomic spheres: LC of radial functions × spherical harmonics
interstitial region: plane waves
Mixed basis
LAPW
DFT: sofwares
the main differences between them

## Slide 35
ParaGauss
PARATEC
PARSEC
PC GAMESS
PLATO
Parallel Quantum Solutions
PWscf (Quantum Espresso)
Q-Chem
SIESTA
Socorro
Spartan
SPR-KKR
TURBOMOLE
VASP
WIEN2k
Abinit
ADF
AIMPRO
Augmented Spherical Wave
Atomistix Toolkit
CADPAC
CASTEP
CP2K
CPMD
CRYSTAL
DACAPO
DALTON
deMon2K
DFT++
DMol3
EXCITING
Fireball
FLEUR
GAMESS (UK)
GAMESS (US)
GAUSSIAN
GPAW
JAGUAR
MOLCAS
MOLPRO
MPQC
NWChem
OpenMX
ORCA
non-exhaustive list
http://en.wikipedia.org/wiki/List_of_quantum_chemistry_and_solid-state_physics_software
DFT: sofwares
the main differences between them
Solid state physics and quantum chemistry

## Slide 36
Part 2
Introduction to the calculation of X-ray absorption spectra
X-ray Absorption Near-Edge Structure
Near-Edge X-ray Absorption Fine Structure

## Slide 37
Basic issue: calculation of the absorption cross section
for a material, i.e., a system of N electrons + Nat nuclei
incident x-ray energy
operator of
the interaction between
x-rays and the system
initial state:
ground state of the system
with energy , degenerescence
final state:
excited state of the system
of energy .
XANES modeling
strong e-- e- interaction
multielectronic approach
ex : L2,3 edges of 3d elements
weak e- - e- interaction
monoelectronic approach (Density Functional Theory)
ex : K edges

## Slide 38
Interaction operator between x-rays and electrons
incident X-ray beam: electromagnetic wave treated as a plane-wave
k: wave vector
: polarization direction
electric dipole transitions (E1)
majority electronic transitions
electric quadrupole transitions (E2)
observable in the K pre-edge of 3d transition elements

## Slide 39
Electric dipole (E1) transitions :
Initial State quantum numbers |  | Edge | final state symmetry
1 | 0 | K | p
2 | 0 | L1 | p
2 | 1 | L2,3 | s+d
3 | 0 | M1 | p
3 | 1 | M2,3 | s+d
3 | 2 | M4,5 | p+f
K or L1
photon energy
L2
photon energy
M4
photon energy
L3
M5
delocalised final state (weak electron repulsion) : p
localized final state (strong electron repulsion) : 3d, 4f
monoelectronic theories (DFT)
multielectronic theories (multiplets)
Interaction operator between x-rays and electrons

## Slide 40
XANES and DFT
monoelectronic empty state (KS)
calculated with a 1s core-hole in the electronic configuration of the absorbing atom
For K edges:
1s atomic orbital

## Slide 41
Note: muffin-tin (MT) potential
ZONE I
ZONE II
MT
ZONE I: atomic spheres
spherical symmetry potentials
ZONE II: interstitial region
constant potential
Full Potential

## Slide 42
XANES and DFT: the calculation codes
2 types
1- Those written to calculate core-level spectra
2- The electronic structure codes, in which a post SCF-process code was added to calculate core-level spectra
at the beginning: multiple scattering (no self-consistency, muffin-tin potential)
continuum, feff, icxanes,….
periodic boundary conditions, reciprocal space
cluster, real space
at the end of the 90’s: finite differences method with fdmnes
currently: fdmnes, feff
Wien2k, CASTEP, Quantum-Espresso (XSpectra), …

## Slide 43
With codes using periodic boundary conditions (for crystals), we have to avoid spurious interaction of the excited atom with its periodically repeated images.
atom with a core-hole
atom without a core-hole
Large interaction
Weak interaction
2x2
supercell
To restore neutrality :
Negative background charge
Excited electron in conduction band
XANES and DFT: periodic boundary conditions and core hole

## Slide 44
XANES and DFT: periodic boundary conditions and core hole
44
unit cell
a = 4.91Å, c = 5.40Å
3 Si 6 O
1×1×1 supercell
= unit cell with 1 core-hole
1 Si* 2 Si 6 O
Si K edge in α-quartz
without core-hole
interaction between core-holes
2×2×2 supercell
a = 9.82Å, c = 10.80Å
1 Si* 23 Si 48 O
convergence

## Slide 45
XANES and DFT: the drawbacks
DFT is dedicated to the calculation of ground state properties
but used here for the modeling of excited states…
possible underestimation of the excitation energies
Static modeling of the core-hole-electron interaction
through the supercell approach or within a cluster of atoms
Exchange and correlation functional is not energy-dependent
inelastic losses not calculated, the convolution factor is a parameter
well identified

## Slide 46
XANES and beyond DFT
GW + Bethe-Salpeter equation (BSE)
TD-DFT (real-space approaches)
Shirley and coll.
Quantum-Chemistry codes: Orca, ADF, Q-chem, …
Olovsson, Puschnig, Ambrosch-Draxl, Lakowski : LAPW
FDMNES
OCEAN interface

## Slide 47
3d0
t2g
eg
3d3
t2g
eg
3d2
t2g
eg
3d6
LS
t2g
eg
3d5
LS
t2g
eg
t2g, eg empty
favorable case
Fe2+
FeS2 pyrite
MbCO protein
single-particle picture
eg empty
acceptable case
Ti4+
TiO2 rutile, anatase
ruby, emerald, spinel:Cr, pyrope:Cr
Cr3+
V3+
grossular:V
Fe3+
MbCN protein
acceptable case
eg empty
t2g, eg empty
critical case
t2g, eg empty
t2g partially empty eg empty
eg empty
t2g partially empty
eg empty
critical case
3d elements in octahedral site
Cabaret et al. PCCP (2010)

## Slide 48
3d0
t2g
eg
single-particle picture
TiO2 rutile, Ti site: centrosymmetric
Cabaret et al. Phys. Chem. Chem. Phys. 12:5619 (2010)
pre-edge : E2 + non local E1
peak A2
local E2 transition 1s 3d eg
+
non-local E1 transition 1s p hybrid. 3d t2g (neighb.)
peak A1
local E2 transition 1s 3d t2g
peak A3
non-local E1 transition 1s p hybrid. 3d eg (neighb.)
Ti4+ in octahedral site

## Slide 49
TiO2 rutile, Ti site: centrosymmetric
pre-edge : E2 + non local E1
0.5 eV
A1 calc. at too high energy !
WHY?
Ti4+ in octahedral site
Cabaret et al. Phys. Chem. Chem. Phys. 12:5619 (2010)
3d0
t2g
eg
single-particle picture

## Slide 50
TiO2 rutile, Ti site: centrosymmetric
pre-edge : E2 + non local E1
dashed: no core-hole
A1 calc. at too high energy !
The 1s core-hole is not attractive enough…
How to improve ?
Ti4+ in octahedral site
3d0
t2g
eg
single-particle picture

## Slide 51
Shirley, J. Electr. Spectr. Rel. Phenom. 136:77 (2004)
Bethe-Salpeter equation
TiO2 rutile, Ti site: centrosymmetric
pre-edge : E2 + non local E1
dashed: no core-hole
Ti4+ in octahedral site

## Slide 52
pre-edge : E2
MgAl2O4:Cr3+, Cr site: centrosymmetric
two E2 peaks (at too high energy…)
Origin?
3d3
t2g
eg
t2g
eg
eg
t2g
A1
A2
single-particle picture
occupied
states
eg
eg
t2g
Cr3+ in octahedral site
Cabaret et al. Phys. Chem. Chem. Phys. 12:5619 (2010)

## Slide 53
pre-edge : E2
Ca3Al2(SiO4)3:V3+, V site: centrosymmetric
Three E2 peaks (at 2eV too high energy…)
Origin?
3d2
t2g
eg
A1
A2
single-particle picture
t2g
eg
eg
t2g
occupied
states
eg
eg
t2g
t2g
A3
V3+ in octahedral site
Cabaret et al. Phys. Chem. Chem. Phys. 12:5619 (2010)

## Slide 54
DFT-GGA
DFT-GGA +U
Juhin et al. PRB 81 (2010)
Angular dependence of core hole screening in LiCoO2
Electronic structure poorly described in GGA
Better described using Hubbard parameter (U) on Co 3d states
Gap = 1.7 eV
Gap =2.3eV

## Slide 55
LiCoO2 : the Co K pre-edge
Best agreement is obtained when including U and the 1s core hole

## Slide 56
LiCoO2 : the Co K pre-edge
pre-edge : E2 + nonlocal E1
Peak a : 1s3d (Co*)
Peak b : 1s4p + O(2p) + Co (3d) n.n. in plane
Peak g : 1s4p + O(2p) + Li (2p)+Co (3d) n.n. out of plane

## Slide 57
3d0 (TiO2) ~ 0.5 eV reduced to 0 using BSE of E. Shirley
3d6 LS (MbCO, FeS2) ~ 0.8 eV
3d3 (Cr-spinel, emerald) 1 ~eV
3d3 (ruby) and 3d2 (V-grossular) 2 ~eV
3d5 LS (MbCN) ~ 1.7 eV
Inherent drawbacks of DFT-LDA/GGA for XANES calculation
electronic repulsion modeling
core hole-electron interaction modeling
E2 and E1 transitions toward 3d (abs) systematically at too high energy
GGA+U reduces 2 eV 1 eV for 3d8 (NiO) Gougoussis et al. PRB 79:045118 (2008)
2.4 eV 1.7 eV for 3d6 LS (LiCoO2) Juhin et al. PRB 81:115115 (2010)
TDDFT+hybrid functionals in Fe complexes : DeBeer et al. J.Phys.Chem.A 112:12936 (2008)
Summary

## Slide 58
However, DFT in LDA/GGA is useful !
number of pre-edge peaks well reproduced
relative intensities and positions in rather good agreement with experiment
single-particle description of transitions with
  E1/E2 character
  degree of local and non-local hybridization
  spin polarization
improved with adding U (NiO, LiCoO2, …)
Inherent drawbacks of DFT-LDA/GGA for XANES calculation
electronic repulsion modeling
core hole-electron interaction modeling
E2 and E1 transitions toward 3d (abs) systematically at too high energy
Summary

## Slide 59
Thank you for your attention.
Thanks to Delphine Cabaret for slide courtesy