## Slide 1
Introduction to XAS
XAS detection techniques
XAS spectral shape
multiplet calculations
X-ray Absorption Spectroscopy

## Slide 2
Element specific
Sensitive to low concentrations
Applicable under extreme conditions
SPACE: Combination with x-ray microscopy
TIME: femtosecond XAS
RESONANCE: RIXS, RPES, R diffraction
X-ray Absorption Spectroscopy
Notes: XAS is element specific because each element has specific binding energies for its core levels.
The XAS edge energy is essentially given by the core level binding energy.

## Slide 3: Interaction of x-rays with matter
XAS, XPS
Elastic scattering (SAXS, XRD)
Inelastic scattering
Mn
X-ray Absorption Spectroscopy

## Slide 4: Interaction of x-rays with matter
X-ray Absorption Spectroscopy
[Rogantini, Astro & Astrophys.609, A22 (1018)]

## Slide 5
Label
Orbital
eV
K
1s
6539
L I
2s
769.1
L II
2p1/2
649.9 [3]
L III
2p3/2
638.7 [3]
M I
3s
82.3 [3]
M II
3p1/2
47.2 [3]
M III
3p3/2
47.2 [3]
X-ray absorption edges
X-ray Absorption Spectroscopy

## Slide 6
Label
Orbital
eV [literature reference]
K
1s
6539 [1]
L I
2s
769.1 [3]
L II
2p1/2
649.9 [3]
L III
2p3/2
638.7 [3]
M I
3s
82.3 [3]
M II
3p1/2
47.2 [3]
M III
3p3/2
47.2 [3]
X-ray absorption edges
X-ray Absorption Spectroscopy
BarKLa
The Nobel Prize in Physics 1917 was awarded to Charles Glover Barkla "for his discovery of the characteristic Röntgen radiation of the elements."

## Slide 7
Label
Orbital
eV [literature reference]
K
1s
6539 [1]
L I
2s
769.1 [3]
L II
2p1/2
649.9 [3]
L III
2p3/2
638.7 [3]
M I
3s
82.3 [3]
M II
3p1/2
47.2 [3]
M III
3p3/2
47.2 [3]
X-ray absorption edges
X-ray Absorption Spectroscopy
sharp
principal
diffuse
fundamental
BarKLa
The Nobel Prize in Physics 1917 was awarded to Charles Glover Barkla "for his discovery of the characteristic Röntgen radiation of the elements."
J. Chem. Educ. 84, 757 (2007)

## Slide 8
X-ray absorption
X-ray Absorption Spectroscopy
Excitation of 3p to 3d state
Lifetime of excitation is short
Lifetime broadening ~200 meV
4sp
3d
O2p
O2s
3p
Notes: 8

## Slide 9
X-ray absorption & x-ray emission
X-ray Absorption Spectroscopy
Decay of 3d electron to 3p core state
X-ray emission
Notes: 9

## Slide 10
X-ray absorption & Auger
Decay of 3d/valence electron to 3p core state
Energy used to excite a 3d/valence electron
Auger electron spectroscopy
X-ray Absorption Spectroscopy
Notes: 10

## Slide 11
X-ray Absorption Spectroscopy
1s core state
Notes: 11

## Slide 12
XAS: detection techniques

## Slide 13
Use decay channels as detector
XAS: detection techniques
Uniform thickness
Uniform concentration of absorbing element
Thin enough for photons

## Slide 14
X-ray penetration lengths &
electron escape depths
100-1000 nm
(CXRO, but 20 nm for L edges)
1-5 nm
XAS: detection techniques

## Slide 15
Use decay channels as detector
XAS: detection techniques
X-ray penetrate 1000 nm (λX)
Electrons escape from 5 nm (λE)
Number of core holes created in first 5 nm is proportional to μ and angle of incidence (α)
ITEY ~ 1 / λX = μX

## Slide 16
Transmission
(pinhole, saturation > thin samples)
Electron Yield
(surface sensitive)
Fluorescence Yield
(saturation & self-absorption:
> dilute samples)
[L edges are intrinsically distorted]
XAS: detection techniques

## Slide 17
Interpretation of spectral shapes
XAS: spectral shape
Notes: 17

## Slide 18
Excitations of core electrons to empty states
The XAS spectra are given by the Fermi Golden Rule
XAS: spectral shape
exciton
edge jump

## Slide 19
Fermi Golden Rule

Excitations to empty states as calculated by DFT
O 1s
XAS: spectral shape (O 1s)
X
Notes: 19

## Slide 20
2p
2s
Phys. Rev. B.40, 5715 (1989)
XAS: spectral shape (O 1s)

## Slide 21
Phys. Rev. B.40, 5715 (1989); 48, 2074 (1993)
XAS: spectral shape (O 1s)
oxygen 1s > p DOS

## Slide 22
Phys. Rev. B. 40, 5715 (1989); 48, 2074 (1993)
XAS: spectral shape (O 1s)

## Slide 23
Final State Rule: Spectral shape of XAS looks like final state DOS
TiSi2
Phys. Rev. B. 41, 11899 (1991)
XAS: spectral shape

## Slide 24
XAS codes:
Multiple scattering: FEFF, FDMNES, etc.
Band structure: WIEN2K, Quantumespresso, etc.
Real-space DFT: ADF, etc.
TiSi2
Phys. Rev. B. 41, 11899 (1991)
XAS: spectral shape

## Slide 25
Iron 1s XAS
2p XAS of transition metal ions
[Phys. Rev. B. 42, 5459 (1990)]
exciton
edge jump
2p > s,d DOS
2p > 3d
(3d5 > 2p53d6, self screened)
X
Notes: 25

## Slide 26
2p3/2
2p1/2
Overlap of core and valence wave functions
 Spectral shape NOT improved in last 30 years!
3d
<2p3d|1/r|2p3d>
XAS: multiplet effects
XAS: spectral shape
[Phys. Rev. B. 42, 5459 (1990)]

## Slide 27
1-particle:
1s edges
(DFT + core hole +U)
many-particle:
open shell systems
(CTM4XAS)
Interpretation of XAS
XAS: spectral shape
Notes: 27

## Slide 28
XAS
1s
DFT
pre-edge
of 3d system
??
2p, 3p,
3d, 4d
multiplets
XAS: spectral shape

## Slide 29
Fe 4p -
Fe 3d 0
O 2p 5
O 2s 20
Fe 3p 50
Fe 3s 85
O 1s 530
Fe 2p 700
Fe 2s 800
Fe 1s 7115
X-ray absorption of a solid
Pre-edges structures in 1s XAS

## Slide 30
3d
N
4p
0
1s
1
3d
N+1
4p
0
pre-edge
edge
1s
1
3d
N
4p
1
Pre-edges structures in 1s XAS
exciton
edge jump

## Slide 31
3d
N
4p
0
1s
1
3d
N+1
4p
0
pre-edge
edge
1s
1
3d
N
4p
1
[Cabaret et al. j. Synchrot. Rad. 6, 258 (1999)]
Pre-edges structures in 1s XAS

## Slide 32
3d
N
4p
0
1s
1
3d
N+1
4p
0
pre-edge
edge
1s
1
3d
N
4p
1
[J. Phys. Cond. Matt. 21, 104207 (2009)]
Pre-edges structures in 1s XAS

## Slide 33
XAS
1s
DFT
pre-edge
of 3d system
2p, 3p,
3d, 4d
multiplets
XAS: spectral shape

## Slide 34
3d XAS of rare earths
4f electrons are localized
No effect of surroundings (no crystal field)
3d XAS is self screened > no charge transfer effect
Initial state
electron-electron interaction.
Valence spin-orbit coupling
Final state
The core hole – valence hole ‘multiplet’ interaction.
The core hole spin-orbit coupling

## Slide 35
3d XAS of rare earths
Nd3+ 4f3 system: ground state is 4I9/2
2S+1LJ term symbols and Hunds rule are explained
in the atomic multiplet pdf file

## Slide 36
Atomic multiplets
2p XAS of NiO with atomic multiplets

## Slide 37
2p XAS of 3d transition metal oxides
3d electrons are less localized
Effect of surroundings (crystal field effect)
3d XAS is self screened > weak charge transfer effect
Initial state
electron-electron interaction.
valence spin-orbit coupling
crystal field effect
Final state
core hole – valence hole ‘multiplet’ interaction.
core hole spin-orbit coupling
crystal field effect

## Slide 38
t2g states
Crystal Field Effects
eg states
crystal field effect

## Slide 39
High-spin or Low-spin
E
T2
E
T2
High-spin 3d5
Low-spin 3d5
crystal field effect: spin state
More in the lecture of Marie-Anne Arrio

## Slide 40
valence e-e interactions Fdd
core-valence e-e Fpd Gpd
core & valence spin-orbit ζ
crystal field 10Dq, Ds, Dt
molecular field, M or H
e-e screening κ
charge transfer Δ, U, Q
hopping TΓ
ionic 3d
(4d, 5d)
4f, 5f
covalent 3d
mixed valence f
ATOMIC
SYMMETRY
BONDING
Multiplet calculations

## Slide 41
valence e-e interactions Fdd
core-valence e-e Fpd Gpd
core & valence spin-orbit ζ
crystal field 10Dq, Ds, Dt
molecular field, M or H
e-e screening κ
charge transfer Δ, U, Q
hopping TΓ
ionic 3d
(4d, 5d)
4f, 5f
3d ions
covalent 3d
mixed valence f
ATOMIC
SYMMETRY
BONDING
Multiplet calculations

## Slide 42
Hubbard U for a 3d8 ground state:
U= E(3d7) + E(3d9) – E(3d8) – E(3d8)
Ligand-to-Metal Charge Transfer (LMCT):
= E(3d9L) – E(3d8)
Charge Transfer Effects
Charge transfer effects

## Slide 43
Charge Transfer Effects
Main screening mechanism in XAS of oxides:
Ligand-to-metal charge transfer
Charge transfer energy  is important for XAS
Hubbard U is NOT important for XAS spectral shape
Charge transfer effects

## Slide 44
3d9L
Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

3d8
Ground State
Charge transfer effects in XAS and XPS
transition metal oxides

## Slide 45

Charge Transfer Effects
3d8
3d9L

## Slide 46

Charge Transfer Effects
3d8
3d9L
9
8

## Slide 47
β 3d8 - α 3d9L
α 3d8 + β 3d9L

Charge Transfer Effects
3d8
3d9L

## Slide 48
E1,2 = ½ [±√(2+4T2)]
=2 and T=0
E1,2 = ½ [2±√(22+0)] = 0 and 2

Charge Transfer Effects
3d8
3d9L

## Slide 49
E1,2 = ½ [±√(2+4T2)]
=2 and T=1
E1,2 = ½ [2±√(22+4)] = 1 ± √2

Charge Transfer Effects
3d8
3d9L

## Slide 50
Charge Transfer Effects in NiO
E(3d9L) – E(3d8) = 
E(3d10LL‘) – E(3d8) = 2
X

## Slide 51
Charge Transfer Effects in NiO
E(3d9L) – E(3d8) = 
E(3d10LL‘) – E(3d8) = 2 +U

## Slide 52
Charge Transfer Effects

## Slide 53
Charge Transfer Effects in NiO
2p XAS: 3d8  2p5 3d9
E (2p53d9) = E2p+  + EL - 9Q

## Slide 54
Charge Transfer Effects in NiO
2p XAS: 3d8  2p5 3d9
E (2p53d9) = E2p+  + EL - 9Q
2p XAS: 3d9L 2p5 3d10L
E (2p53d10L) = E2p+2+U + EL -10Q

## Slide 55
Charge Transfer Effects in NiO
2p XAS: 3d8  2p5 3d9
E (2p53d9) = E2p+  + EL - 9Q
2p XAS: 3d9L 2p5 3d10L
E (2p53d10L) = E2p+2+U + EL -10Q
Energy difference: FINAL = +U-Q   -1 eV

## Slide 56

+U-Q
Charge Transfer Effects in XAS

## Slide 57
3d9L
3d8
NiO: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

2p53d10L
2p53d9
+U-Q  
Charge Transfer Effects
Charge transfer effects

## Slide 58
β 3d8 - α 3d9L
α 3d8 + β 3d9L

+U-Q  
β’ c3d9 – α’ c3d10L
α' c3d9 + β’ c3d10L
~0
~1
Intensity bonding combination: [α α’+ β β’]2
α  α’  α2+ β2 =1
Charge transfer effects

## Slide 59
β 3d5 - α 3d6L
α 3d5 + β 3d6L

+U-Q  
β’ c3d6 – α’ c3d7L
α' c3d6 + β’ c3d7L
~0
~1
Intensity anti-bonding combination:α β’- β α’
α  α’  αβ - βα =0
Charge transfer effects

## Slide 60
Neutral experiments are self-screened
XAS, optical, EPR, EELS, RIXS
>> small satellites
>> crystal field theory can be used
Ionising experiments are not self-screened
XPS, Auger,
>> large screening > large satellites
>> crystal field theory can not be used
Charge Transfer Effects
Charge transfer effects

## Slide 61
3d6L
Transition metal oxide: Ground state: 3d5 + 3d6L
Energy of 3d6L: Charge transfer energy 
XAS
2p53d7L
+U-Q  

2p53d6
3d5
2p53d6L
XPS
2p53d5
-Q
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 62
3d9L
3d8
NiO: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

2p53d10L
2p53d9
+U-Q  
Charge Transfer Effects
Charge transfer effects

## Slide 63
Tanabe-Sugano with Charge transfer
α 3d8 + β 3d9L
Tanabe-Sugano diagrams with charge transfer
NiO
Cu3+

## Slide 64
=10
NiO
La2Li½Cu½O4
30% 3d8
1A1
30% 3d8
3A2
=-5
=5
=0
=-10
3d8 + 3d9L
Charge Transfer effects
Chem. Phys. Lett. 297, 321 (1998)
Charge transfer effects in XAS

## Slide 65
3d6L
3d5

2p53d7L
2p53d6
+U-Q  
FeIII: Ground state: 3d5 + 3d6L
LMCT and MLCT:  - bonding
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)

## Slide 66
3d4L
3d6L
3d5
FeIII: Ground state: 3d5 + 3d6L + 3d4L

2p53d5L
2p53d7L
2p53d6
+U-Q   - 2

-U+Q   + 2
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 67
FeIII(tacn)2
FeIII(CN)6
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 68
Multiplet calculations
Calculated for an atom/ion
Valence and core spin-orbit coupling
Core and valence electron-electron interaction.
Comparison with experiment
Core hole potential and lifetime
Local symmetry (crystal field)
Spin-spin interactions (molecular field)
Core hole screening effects (charge transfer)
Notes: 68

## Slide 69
First Principle Multiplet calculations
Calculated for an atom/ion
Valence and core spin-orbit coupling
Core and valence electron-electron interaction.
Comparison with experiment
Core hole potential and lifetime
Local symmetry (crystal field)
Spin-spin interactions (molecular field)
Core hole screening effects (charge transfer)
Notes: 69

## Slide 70
2p XAS first-principle codes
SOLIDS
Band structure multiplet (Haverkort, Green, Hariki)
Cluster DFT multiplet (Ikeno, Ramanantoanina, Delley)
MOLECULES
Restricted Active Space CI (Odelius, Kuhn)
Restricted Open-shell CI (Neese)
TDDFT/BSE
Time-Dependent DFT (Joly)
Bethe-Salpeter (Rehr, Shirley)
Multi-channel Multiple-scattering (Kruger)
Notes: 70

## Slide 71
Iron 1s XAS
Overview
XAS
MCD
XPS
RIXS
Notes: 71

## Slide 72
Iron 1s XAS
2p XAS
X
I(w)
Γ2p= 0.2 eV
Notes: 72

## Slide 73
Iron 1s XAS
2p XMCD
X
I+(w)- I-(w)
Γ2p= 0.2 eV
Left and right polarized x-rays
Notes: 73

## Slide 74
Iron 1s XAS
2p XPS
I(Ek)
Γ2p= 0.2 eV
(additional broadening)
Large screening
Notes: 74

## Slide 75
Iron 1s XAS
2p3d RIXS
X
I(w,w’)
Fixed energy loss
Electronic, magnetic, vibrational
Γ3d= 10 meV?
Notes: 75