## Slide 1
Resonant Inelastic X-ray Scattering
core-core RIXS
core-valence RIXS
RIXS

## Slide 2
Resonant Inelastic X-ray Scattering
Resonant X-ray Raman Scattering (RXRS)
Resonant X-ray Emission Spectroscopy (RXES)
Resonant X-ray Energy Loss Spectroscopy (R-XELS)
RIXS

## Slide 3
Ψ0
Core-core RIXS
2p
electronic
dd, CT
magnon
vibrations
3s

## Slide 4
Resonant Inelastic X-ray Spectroscopy
2p XAS of CaF2
3d0

’
3s13d1
2p53d1
2p3s RIXS of CaF2

## Slide 5
2p3s RIXS of CaF2
Ground state is 3d0
Excitation (i0) 3d0  (x) 2p53d1
Decay (x) 2p53d1  (f) 3s13d1
2p3s RIXS of CaF2

## Slide 6
Resonant Inelastic X-ray Scattering
2p3s RIXS of CaF2

## Slide 7
Phys. Rev. B.
53, 7099 (1996)
Resonant Inelastic X-ray Scattering
3d0

’
3s13d1
2p53d1
2p3s RIXS of CaF2

## Slide 8
Ψ0
1s2p RIXS of transition metal ions
1s
electronic
dd, CT
magnon
vibrations
2p

## Slide 9
CoIII(acac)
K edge and 1s2p RIXS
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
1s2p RIXS of transition metal ions

## Slide 10
CoIII(acac)
K edge and 1s2p RIXS
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
1s2p RIXS of transition metal ions

## Slide 11: Pre-edge and edge
Only quadrupole peaks visible
3d7  1s13d8  2p53d8
CoO
high-spin CoII
3d7 [4T2]
Sharper pre-edge structures in 1s XAS

## Slide 12
Co K edge of LiCoO2
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
K pre-edge of TM oxides (LiCoO2)
Pre-edges structures in 1s XAS

## Slide 13
Co K edge of LiCoO2
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
K pre-edge of TM oxides (LiCoO2)
Pre-edges structures in 1s XAS

## Slide 14
K pre-edge of TM oxides
Pre-edges structures in 1s XAS

## Slide 15
K pre-edge of TM oxides
Pre-edges structures in 1s XAS
J. Phys. Cond. Matt. 21, 104207 (2009); Phys. Rev. B. 81, 115115 (2010)

## Slide 16
K edge and 1s2p RIXS
Hard x-ray RIXS
Reduce lifetime from 1.5 to 0.2 eV (HERFD XANES)
Reveal new features at pre-edge
Soft x-ray edges with hard x-rays
Spin-polarized XAS
Range extended EXAFS
Background free FY for low conc.
RIXS-MCD

## Slide 17
Quadrupole to 3d-states
Dipole to 4p-states
Decay of 2p-electron into 1s-hole
Final state identical to 2p XAS
Resonant Inelastic X-ray Scattering
1s2p RIXS of Fe2O3
RIXS: soft x-ray edge with hard x-rays

## Slide 18
1s2p RIXS
2p-XAS
Phys. Rev. B.
58, 13452 (1998)
Resonant Inelastic X-ray Scattering
1s2p RIXS of Fe2O3
RIXS: soft x-ray edge with hard x-rays

## Slide 19: Chemical Dependence of Kb Emission
Experiment
Theory
Equal center-of-gravity energies used in calculations!
Selective XAS
RIXS: selective XAS

## Slide 20
Inorg. Chem.
41, 3121 (2002)
Selective XAS
RIXS: selective XAS

## Slide 21
RIXS: range extended EXAFS
Lanthanum edges relative close in energy
Only short EXAFS region possible
Use partial FY: see only one edge
Glatzel ea, Phys. Rev. B. 72, 014117 (2005)

## Slide 22
Glatzel ea, Phys. Rev. B. 72, 014117 (2005)
Extra absorption at new edge
Probing depth is changing
Only works for dilute samples
RIXS: range extended EXAFS

## Slide 23
Core-valence RIXS

## Slide 24
Ψ0
3 2 1 0
2p3d RIXS of transition metal ions
core
electronic
dd, CT
magnon
vibrations

## Slide 25
Resonant Inelastic X-ray Scattering

## Slide 26
resonant inelastic x-ray spectroscopy
Notes: 26

## Slide 27
NiII 3d8 []  2p53d9[jj]  3d8[]
2p3d RIXS of NiO
Notes: Cartoon of a spin-flip transition

## Slide 28
dd
spin-flip
‘spin-flip’
MS
S
Phys. Rev. B. 57, 14584 (1998)
2p3d RIXS of NiO
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 29
2p3d RIXS
eV
electron-electron
crystal field
charge transfer
polarization, angles
(in, sample, out)
meV
spin-orbit, magnetic
distortions
vibrations
RIXS 2018: 30 meV
RIXS1998: 500 meV
Notes: 29

## Slide 30
Energy dependence in 2p3d RIXS
In 2p3d RIXS the intensity of charge transfer is smaller than dd-excitations
[Ament et al., Rev. Mod. Phys. 83, 705 (2011)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 31
Energy dependence in 2p3d RIXS
2 eV – 10 eV
charge transfer
0.0 eV – 6 eV
dd excitations (atomic + crystal field)
0.0 – 0.5 eV
spin-flip (magnon)
symmetry distortions
HS-LS transition point
spin-orbit coupling
vibrations (phonon)
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 32
2p3d RIXS
2p3d RIXS in cuprates
Schlappa et al., Nature (2012)
Bisogni et al., arXiv:1310.8346
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 33
Select specific states in 2p3d RIXS (Fe3O4)
exchange
spin-orbit + exchange
[Huang et al. Nature Comm. 8, 15929 (2017) ]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 34
Select specific states in 2p3d RIXS (Fe3O4)
exchange
spin-orbit + exchange
Interference shows that lifetime broadening
(fwhm) is only 100 meV, not 200 meV
20 fs >>> 40 fs
[Huang et al. Nature Comm. 8, 15929 (2017) ]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 35
[CoIIW12O40]·
[Van Schooneveld, Hunault et al., unpublished ]
2p3d RIXS of isolated chromium ions (ruby)

## Slide 36
Multiplet challenge: 2p3d RIXS on Cr3+
Notes: 36

## Slide 37
Multiplet challenge: 2p3d RIXS on Cr3+
[Hunault, van Schooneveld, submitted]
Optical resolution can be 0.01 meV
Spin-forbidden dd-excitations limited by experimental resolution
Notes: 37

## Slide 38
Spin-state in LaCoO3 (single crystal)
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 39
Spin state of LaCoO3
E
T2
E
T2
5T2
1A1
E
T2
3T1
NOTE: Term symbols and orbital occupations are only indications: they are mixed by electron-electron, spin-orbit, etc.
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 40
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
dd-excitations + fluorescence
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 41
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
dd-excitations + fluorescence
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 42
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
dd-excitations + fluorescence
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 43
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 44
Spin state of LaCoO3
[Tomiyasu et al. PRL 8, 119, 196402 (2017) ]
Spin transition is from low-spin to high-spin,
. . . . but is it really high-spin?
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 45
Spin state of LaCoO3
[Sotnikov & KUnes, Sci. Rep 6, 30510 (2016); Wang et al. submitted ]
Order of states at zero Kelvin: LS < HS < IS
Strong coupling between LS and IS (not with HS)
Large dispersion of IS: Excitonic Insulator
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 46
Spin state of LaCoO3
[Wang et al. submitted ]
q-dependent RIXS with 90 meV resolution at 20 K
[data treatment: remove fluorescence and isolate states related to the triplet states (IS)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 47
Spin state of LaCoO3
[Wang et al. submitted ]
q-dep. RIXS
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 48
Spin-state in LaCoO3 (thin films)
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 49
LaCoO3 thin films
Synthesis: Pulsed laser deposition in
combination with in situ monitoring by RHEED
Samples: 4nm (10 ML) and 60 nm films
LaCoO3/LaAlO3 and LaCoO3/SrTiO3
[PLD @ Twente University (Gertjan Koster) ]
Notes: In order to have a good comparison, we considered three different kind of strains.
First is the relaxed one, with is LaCoO3 crystal.
Then we have the LaCoO3 films grown on the SrTiO3 and LaAlO3.
They are presented two different strained style.

## Slide 50
In-plane
tensile
strained
In-plane
compressive
strained
Single crystal
LaCoO3 thin films
LaCoO3/LaAlO3
LaCoO3/SrTiO3
Notes: In order to have a good comparison, we considered three different kind of strains.
First is the relaxed one, with is LaCoO3 crystal.
Then we have the LaCoO3 films grown on the SrTiO3 and LaAlO3.
They are presented two different strained style.

## Slide 51
LaCoO3 thin films
Notes: In order to have a good comparison, we considered three different kind of strains.
First is the relaxed one, with is LaCoO3 crystal.
Then we have the LaCoO3 films grown on the SrTiO3 and LaAlO3.
They are presented two different strained style.

## Slide 52
LaCoO3 thin films
Notes: In order to have a good comparison, we considered three different kind of strains.
First is the relaxed one, with is LaCoO3 crystal.
Then we have the LaCoO3 films grown on the SrTiO3 and LaAlO3.
They are presented two different strained style.

## Slide 53
relaxed
5B2
LaCoO3 thin films
5B2

## Slide 54
Spin state of LaCoO3
Single Crystal:
Low spin at 20 Kelvin.
Gas of mobile bosonic (IS) excitons
HS states are bound bi-excitons
Thin films:
Interface induced stress → high-spin ground states
LaCoO3/SrTiO3 has 5B2 ground state
LaCoO3/LaAlO3 has 5E ground state
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 55
2p core hole in 3d metal ions decays for 80+% by 2p3d x-ray emission
2p3d RIXS analysis has implications for fluorescence yield detection
Yield detection

## Slide 56
Electron yield
Fluorescence Yield (1. dilute limit)
FY (2. state dependent decay)
No XMCD sum rules in FY
FY (3. inverse PFY)
FY (4. dips and peaks)
Yield detection

## Slide 57
X-ray enters sample
Total absorption
Penetration depth λ is inverse proportional to
Yield detection
λ

## Slide 58
Core hole decays by photons (σ) or electrons (σE)
Electrons escape from surface determined by their kinetic energy λ
Electron yield: EY = * σE * λ ~
[Neglect angular dependences]
Electron Yield detection
λ
λ

## Slide 59
Electron Yield detection

## Slide 60
Core hole decays by photons (σ) or electrons (σE)
Photons escape prop. to λ’= ]
Fluorescence yield: FY = * σ * λ
[Neglect angular dependences]
Fluorescence Yield detection
λ

## Slide 61
Fluorescence yield: FY = * σ * λ
= +
λ ~1/
σ is different for edge and background (σB)
Fluorescence Yield detection
ITFY ~

## Slide 62
FY detection of dilute sample
ITFY ~
ITFY ~
ITFY ~

## Slide 63
Fluorescence Yield
“saturation & self-absorption”
De-saturation software
(μ(ω) based on CRXO)
FY detection of non-dilute sample

## Slide 64
Single synchrotron pulselength is too long
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
XAS of radiation sensitive sample
Notes: 64

## Slide 65
FY-XAS of radiation sensitive sample
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Fluorescence does not measure XAS spectrum
Saturation ?
Notes: 65

## Slide 66
FY-XAS of radiation sensitive sample
Fluorescence does not measure XAS spectrum
NO Saturation
State-dependent decay
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 66

## Slide 67
Yield methods assume a constant ratio between radiative and non-radiative decay
If this ratio is state (= energy) dependent then the related yield methods do not measure XAS.
The dominant yield method is not visibly affected, thus for soft X-rays only FY is affected, not electron yield.
FY detection: State dependent decay

## Slide 68
FY detection: State dependent decay
FY
EY
L3
L2
Solid State Comm. 92, 991 (1994)

## Slide 69
FY detection (state-dependent, dilute)
ITFY ~
ITFY ~
Main decay of 2p core hole is 2p3d RIXS
Integrate RIXS spectrum to 2p3d PFY
TFY ~ 2p3d PFY
NOTE: “RIXS” has angular dependence effects

## Slide 70
XAS: transmission & FY
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 70

## Slide 71
FY-XAS ≠ XAS L2 edge increases High-energies increase
Fluorescence Yield detection
Kurian J. Phys. Cond. Matt. 24, 435602 (2012)

## Slide 72
XMCD sum rules break down
Ni/Co 20%, Fe 30%, Mn > 100% error
Fluorescence Yield XMCD
Liu ea, Phys. Rev. B. 96, 054446 (2017)

## Slide 73
ITFY ~ = the integrated RIXS
Measure the partial fluorescence yield of the background.
IBFY ~
1/(1+x) ≈ 1 – x
IBFY ≈ 1 –
Measure a negative XAS spectrum, essentially tracking the probing depth [λ]
FY detection: 3 inverse PFY

## Slide 74
FY detection: 3 inverse PFY
Achkar ea, scientific reports 1, 82 (2011)

## Slide 75
FY detection: 4 dips and peaks
Measure the total fluorescence yield
State-dependent decay modified metal PFY
+ Negative IPFY
ITFY ~
ITFY ~ c1

## Slide 76
FY detection: 4 dips and peaks
Nature Chem. 4, 766 (2012) & Phys. Rev. Letter discussions (2014)