## Slide 1
Fluorescence Yield detection
XPS
Ground state analysis

## Slide 2
FY (1. dilute limit)
FY (2. state dependent decay)
FY (3. inverse PFY)
FY (4. dips and peaks)
Fluorescence Yield detection

## Slide 3
X-ray enters sample
Total absorption
Penetration depth λ is inverse proportional to
λ
Fluorescence Yield detection

## Slide 4
Core hole decays by photons (σ) or electrons (σE)
Photons escape prop. to λ’= ]
Fluorescence yield: FY = * σ * λ
[Neglect angular dependences]
Fluorescence Yield detection
λ

## Slide 5
Fluorescence yield: FY = * σ * λ
= +
λ ~1/
σ is different for edge and background (σB)
Fluorescence Yield detection
ITFY ~

## Slide 6
FY detection of dilute sample
ITFY ~
ITFY ~
ITFY ~

## Slide 7
Fluorescence Yield
“saturation & self-absorption”
De-saturation software
(μ(ω) based on CRXO)
FY detection of non-dilute sample

## Slide 8
Single synchrotron pulselength is too long
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
XAS of radiation sensitive sample
Notes: 8

## Slide 9
FY-XAS of radiation sensitive sample
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Fluorescence does not measure XAS spectrum
Saturation ?
Notes: 9

## Slide 10
FY-XAS of radiation sensitive sample
Fluorescence does not measure XAS spectrum
NO Saturation
State-dependent decay
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 10

## Slide 11
Yield methods assume a constant ratio between radiative and non-radiative decay
If this ratio is state (= energy) dependent then the related yield methods do not measure XAS.
The dominant yield method is not visibly affected, thus for soft X-rays only FY is affected, not electron yield.
FY detection: State dependent decay

## Slide 12
FY detection: State dependent decay
FY
EY
L3
L2
Solid State Comm. 92, 991 (1994)

## Slide 13
FY detection (state-dependent, dilute)
ITFY ~
ITFY ~
Main decay of 2p core hole is 2p3d RIXS
Integrate RIXS spectrum to 2p3d PFY
TFY ~ 2p3d PFY
NOTE: “RIXS” has angular dependence effects

## Slide 14
XAS: transmission & FY
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 14

## Slide 15
FY-XAS ≠ XAS L2 edge increases High-energies increase
Fluorescence Yield detection
Kurian J. Phys. Cond. Matt. 24, 435602 (2012)

## Slide 16
XMCD sum rules break down
Ni/Co 20%, Fe 30%, Mn > 100% error
Fluorescence Yield XMCD
Liu ea, Phys. Rev. B. 96, 054446 (2017)

## Slide 17
ITFY ~ = the integrated RIXS
Measure the partial fluorescence yield of the background.
IBFY ~
1/(1+x) ≈ 1 – x
IBFY ≈ 1 –
Measure a negative XAS spectrum, essentially tracking the probing depth [λ]
FY detection: 3 inverse PFY

## Slide 18
FY detection: 3 inverse PFY
Achkar ea, scientific reports 1, 82 (2011)

## Slide 19
FY detection: 4 dips and peaks
Measure the total fluorescence yield
State-dependent decay modified metal PFY
+ Negative IPFY
ITFY ~
ITFY ~ c1

## Slide 20
FY detection: 4 dips and peaks
Nature Chem. 4, 766 (2012) & Phys. Rev. Letter discussions (2014)

## Slide 21
XPS

## Slide 22
I(FIXED)
X-ray absorption and X-ray photoemission
XAS and XPS

## Slide 23
3d6L
Transition metal oxide: Ground state: 3d5 + 3d6L
Energy of 3d6L: Charge transfer energy 
XAS
2p53d7L
+U-Q  

2p53d6
3d5
2p53d6L
XPS
2p53d5
-Q
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 24

+U-Q
Charge Transfer Effects in XAS
Charge transfer effects in XAS

## Slide 25
Charge transfer
Charge transfer effects in XAS
XAS = neutral
Self screened
Small charge transfer satellites

## Slide 26

-Q
Charge Transfer Effects in XPS
Charge transfer effects in XPS

## Slide 27
Charge transfer effects in XPS
Charge transfer effects in XPS
XAS = neutral
Self screened
Small charge transfer satellites
XPS = ionising
Large screening
Large charge transfer satellites

## Slide 28
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 29
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 30
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 31
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 32
Resonant Auger of NiO

## Slide 33
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)

## Slide 34
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)
3d8 → 2p53d9
2p53d9 → 3s03d9ε

## Slide 35
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)
3d8 → 2p53d9
3d9L→ 2p53d10L
2p53d9 → 3s03d9ε
2p53d10L → 3s03d10ε
ONLY 2 PEAKS

## Slide 36
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)

## Slide 37
Resonant Auger of NiO
Phys. Rev. B. 59, 9933 (1999)

## Slide 38
Resonant Auger of NiO

## Slide 39
Ground state analysis

## Slide 40
    Term symbols with maximum spin S are lowest in energy,
    Among these terms: Term symbols with maximum L are lowest in energy
    In the presence of spin-orbit coupling, the lowest term has
    J = |L-S| if the shell is less than half full
    J = L+S if the shell is more than half full
Hunds rules

## Slide 41
    max S > max L > max J (if more than half full)
    What is the Hund’s rule ground states for 3d2 ?
Hunds rules
2  | 1  | 0  | -1  | -2 
2  | 1  | 0  | -1  | -2 

## Slide 42
    max S > max L > max J (if more than half full)
    What is the Hund’s rule ground states for 3d2 ?
Hunds rules
2  | 1  | 0  | -1  | -2 
2  | 1  | 0  | -1  | -2 
L=3, S=1
J=2 Term symbol = 3F2

## Slide 43
    max S > max L > max J (if more than half full)
    What is the Hund’s rule ground states for 3d2 ?
Hunds rules
2  | 1  | 0  | -1  | -2 
2  | 1  | 0  | -1  | -2 

## Slide 44
    What is the Hund’s rule ground states for 3d2 ?
Hunds rules

## Slide 45
Energy
Symmetries Oh
Total symmetry
1S
4.6 eV
1A1
3P
0.2 eV
3T1
1D
-0.1 eV
1E + 1T2
3F
-1.8 eV
3A2 + 3T1 + 3T2
1G
0.8 eV
1A1+1T1+1T2+1E
Crystal Field Effects on 3d8 states

## Slide 46
Crystal Field Effects: Tanabe-Sugano

## Slide 47
Tanabe-Sugano with Charge transfer
α 3d8 + β 3d9L

## Slide 48
48
CTM4DOC
[Delgado et al. J. Synchrot. Rad 23, 1264 (2016)]

## Slide 49
49
CTM4DOC
+ charge transfer
+ translation symmetry
[Delgado et al. J. Synchrot. Rad 23, 1264 (2016)]

## Slide 50
50
CTM4DOC

## Slide 51
51
CTM4DOC