## Slide 1: Polarization and dichroism in X-ray Absorption Spectroscopy
Heba Elnaggar
CNRS, Sorbonne University
Hebatalla.elnaggar@sorbonne-universite.fr
Hands on spectroscopy calculations of quantum material - Heidelberg

## Slide 2: Dichroism
Dichroism:
Difference of the propagation of light measured with
two orthogonal polarization
states of the incoming light
Avoid glare (LH light)
Notes: I think most of us are familiar with dichroism in the optical regime from our daily lives. For example from polarized glasses and how it avoids glare.
Glare tends to happen when lightwaves strike a flat surface, causing the light to reflect, or bounce off the surface, in a horizontal manner (brewster law). This causes the light to be intense, which can hurt the eyes and make it more difficult to see.
The filters on polarized lenses absorbs LH light and hence stops the glare.

## Slide 3: Introduction to X-ray dichroism
Linear Dichroism (LD):
Difference measured with LH / LV
Circular Dichroism (CD):
Difference measured with CR / CL
Natural Dichroism (ND):
Difference in magnetic system
Measurement:
Origin:
Magnetic Dichroism (MD):
Difference in structurally distorted system
Magneto-chiral Dichroism (MχD):
Difference in a magnetic + chiral system
And more …
Notes: So similar to the optical regime, dichrosim effect is also present in the x-ray regime.
And there are many different types of dichroism and classifications.
For example, it can be classified according to the measurement. So in this case we can say that it is linear dichroism when it is measured with linear light.

## Slide 4: Why do we need X-ray dichroism?
The measurement of dichroism is often challenging…
  Control polarization, orientation of sample, single crystals required, several measurements …
but provides access to properties that can be lost in the average measurements!
How can we calculate X-ray polarization dependence and dichroism?
X-ray Linear Dichroism (XLD)
X-ray Magnetic Circular Dichroism (XMCD)
Can we predict all X-ray dichroism effects?
What we will discuss:

## Slide 5
How can we calculate XAS polarization dependence?

## Slide 6: How do we calculate XAS dichroism?
Final state
Initial state
Transition operator
Fermi golden rule!

## Slide 7: How do we calculate XAS dichroism?
Polarization vector
Position vector
Wave vector
Taylor expansion:
Dipole
Quadrupole

## Slide 8: Dipole transition operator
Expression in terms of l=1 spherical harmonics (p orbitals):
Dipole:
Examples: transition operator used for L2,3 edges and K-edges
Defined wrt to the crystal axes

## Slide 9: Quadrupole transition operator (e.g. K edge of TM)
Quadrupole:
Expression in l=2 spherical harmonics (d orbitals):
Available in a Mathematic Notebook!
Examples: transition operator used for K pre-edges

## Slide 10
X-ray Linear Dichroism (XLD)

## Slide 11: X-ray Linear Dichroism in Oh Cu2+
eg:(dx2- y2, dz2)
t2g:(dxy, dzy, dzx)
HOLE: ~
Cu2+ Ion
d9

## Slide 12: X-ray Linear Dichroism in Oh Cu2+
3d electron
(think d orbitals)
2p electron
(think p orbitals)
Dipole
(think px orbitals)
<f¦ | T | ¦i>
y
z
x
z
x
y
y
z
x
z
x
y

## Slide 13: X-ray Linear Dichroism in Oh Cu2+
Dipole
(think p orbitals)
<f¦ | T | ¦i>
y
z
x
z
x
y
y
z
x
z
x
y
2p electron
(think p orbitals)
3d electron
(think d orbitals)

## Slide 14: X-ray Linear Dichroism in Oh Cu2+
2p electron
(think p orbitals)
3d electron
(think d orbitals)
Dipole
(think p orbitals)
<f¦ | T | ¦i>
y
z
x
z
x
y
y
z
x

## Slide 15: X-ray Linear Dichroism in Oh symmetry
Quanty Calculation of L2,3 XAS of Oh Cu2+
Experimental results of K-edge XAS of Oh Cr3+ in MgAl2O4
Dipole: p -> d
Dipole: s -> p
Juhin et. al., Phys. Rev. B 78, 195103, 2008
Dipole transition in Oh symmetry are isotropic !

## Slide 16: Dipole XLD in reduced symmetry
Cu2+ Ion
a1g:(dz2)
b2g:(dxy)
d9
eg:( dzy, dzx)
b1g:(dx2- y2 )
HOLE: ~
Elongated Oh

## Slide 17: X-ray Linear Dichroism in D4h Cu2+
Dipole
(think p orbitals)
<f¦ | T | ¦i>
z
x
y
z
x
y
2p electron
(think p orbitals)
3d electron
(think d orbitals)

## Slide 18: X-ray Linear Dichroism in D4h Cu2+
Dipole
(think p orbitals)
18
<f¦ | T | ¦i>
z
x
y
z
x
y
2p electron
(think p orbitals)
3d electron
(think d orbitals)

## Slide 19: X-ray Linear Dichroism in D4h Cu2+
2p electron
(think p orbitals)
3d electron
(think d orbitals)
Dipole
(think p orbitals)
<f¦ | T | ¦i>
z
x
y

## Slide 20: X-ray Linear Dichroism in D4h symmetry
Quanty Calculation of L2,3 XAS of D4h Cu2+
Experimental results of L2,3 XAS of D4h Fe2+
Dipole transition in lower symmetries give rise to X-ray Linear Dichroism
XAS is proportional to the #holes
XLD tells us which holes are these
Schofield et. al., Miner. B 62, 65, 1998

## Slide 21
X-ray Magnetic Circular Dichroism (XMCD)

## Slide 22: X-ray Magnetic Circular Dichroism (XMCD)
Thole et. al., Phys. Rev. lett. (1992). 68
B
B
For ferro/ferri-magnetic materials
At L3,2 edges:
Valence band has a spin-imbalance due to the magnetic ordering
Right- and left-circularly polarized photons carry opposite momentum (+1, -1)
Angular momentum of the photon interacts with the spin of the electron by means of the SOC
Notes: Angular momentum of the photon interacts with the spin of the electron by means of the SOC (Fano effect).
◮ Right- and left-circularly polarized photons carry opposite momentum ⇒ there is a spin imbalance in the photocurrent produced by the right- and left-circularly polarized x-rays.
2. Valence band acts as a spin detector for the (spin-imbalanced) photocurrent.

## Slide 23: XMCD in CoFe2O4
Sum rules:
Relate dichroism to the average ground state magnetic moment
Experimental results of Fe L2,3 XMCD

## Slide 24: Sum Rules for XMCD
XAS
XMCD
XMCD
XMCD ∼ average orbital magnetic moment
Isotropic ∼ number of holes
XMCD ∼ average spin magnetic moment
Thole et. al., Phys. Rev. lett, 68, 1992
Notes: One can deduce ground state proper

## Slide 25: However …
Issues to consider:
Background removal
(edge position, mixing of edges, detection mode “FY?”)
Can be calculated by Quanty!
Magnetic dipole term
Notes: Tz : provides a measure of the anisotropy of the field of the spins when the atomic cloud is distorted, either by the spin-orbit interaction or by crystal-field effects [7].

## Slide 26
What other dichroism effects exist?
Can we describe them in a compact way?

## Slide 27: General expression of the XAS
Off-diagonal: ->
y polarized light is changed by the system to an x polarized
Low symmetry system or magnetic system
Rank 1 tensor
Rank 2 tensor:
TX - TX | TX - TY | TX - TZ
TY - TX | TY - TX | TY - TZ
TZ - TX | TZ - TY | TZ - TZ

## Slide 28: X-ray Linear Dichroism
Slide: M. W. Haverkort
D4h

## Slide 29: X-ray Magnetic Circular Dichroism
XMCD= i
Slide: M. W. Haverkort
Magnetism breaks time reversal symmetry.
This results in the asymmetry of the off-diagonal elements

## Slide 30: The full XAS Tensor
We can compute all possible dichroisms from the conductivity tensor!
Maximum of nine spectra required in the most general case
Slide: M. W. Haverkort

## Slide 31
Can we measure the full XAS tensor?

## Slide 32
Magnetite: [Fe3+]Td [Fe2+ , Fe3+]OhO4
Magnetite: Fe L3,2-edge XAS
Ferrimagnetic system:
  We expect to measure XMCD and that the tensor has off-diagonal elements
The Fe2+ Oh are distorted to D3d:
  We expect to measure XLD and that the tensor has different components in various directions

## Slide 33
To get all elements:
9 independent measurements
Linear polarization (diagonals + symmetric off diagonals)
Circular polarization (asymmetric off diagonals)
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Magnetite: Fe L3,2-edge XAS
Imaginary: measured
Real: transformation

## Slide 34
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Building the tensor

## Slide 35
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Nine linear independent measurements to construct the full tensor
Building the tensor

## Slide 36
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Diagonal Elements:
is different
XMLD in dipole cubic
symmetry due to magnetism!
Analyzing the tensor: Diagonal XMLD

## Slide 37
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Off-diagonal Elements:
gives XMCD
XMCD in cubic symmetry
Analyzing the tensor: XMCD

## Slide 38
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Off-diagonal Elements:
10x less but not 0!
XMLD signature of small non-cubic distortion leading to mixing of x-z direction
Analyzing the tensor: small distortion

## Slide 39
Elnaggar et. al., J. Synchrotron Rad. (2021). 28, 247–258
Nine linear independent measurements to construct the full tensor
All dichroism effects in your system

## Slide 40
Dichroism holds a lot of information about the system which is wasted when we only look on the average
There are many dichroism signals (e.g., magnetic, structural, chiral, linear, circular,…)
Analysing the symmetry of our system is a great tool to predict which dichroism signals to expect (e.g. cubic no dichroism for dipole transitions, …)
XMCD + sum rules relate the spectra to ground state properties (e.g., spin and orbital moments) which is a powerful quantitative tool to study magnetism.
We can describe all the dichroism effects in a system in a compact way using the tensor expression of the XAS cross-section
Concluding Remarks

## Slide 42
Can we regroup the conductivity tensor to more transparent terms?

## Slide 43
Fe3O4 : Creating a Spherical Tensor (rank 2)
Create linear combination based on spherical symmetry
Rank 0 --> Isotropic

## Slide 44
Fe3O4 : Creating a Spherical Tensor (rank 2)
Create linear combination based on spherical symmetry
Rank 1 --> circular dichroism, 3 terms

## Slide 45
Fe3O4 : Creating a Spherical Tensor (rank 2)
Create linear combination based on spherical symmetry
Rank 2 --> Linear dichroism, 5 terms

## Slide 46
How is all this helpful?

## Slide 47
Fe3O4: Quantifying Magnetic Moments from XMCD
Elnaggar et. al., Phys. Rev. Mat. (2020). 4, 024415
Magnetite: [Fe3+]Td [Fe2+ , Fe3+]OhO4

## Slide 48
Fe3O4: Quantifying Small Distortion from XMLD
Trigonal distortion
Dσ = 0.1 eV
Magnetite: [Fe3+]Td [Fe2+ , Fe3+]OhO4
Elnaggar et. al., Phys. Rev. Mat. (2020). 4, 024415
XMLD has two effects:
Structure
Magnetic

## Slide 49
Fe3O4: Quantifying Small Distortion from XMLD
Magnetite: [Fe3+]Td [Fe2+ , Fe3+]OhO4
Elnaggar et. al., Phys. Rev. Mat. (2020). 4, 024415
Tetragonal
Trigonal