## Slide 1
Ψ0
Core level
electronic
dd, CT
magnon
phonon
RIXS and excited states
1000 eV
1 eV
100 meV

## Slide 2
Ψ0
Core level
electronic
dd, CT
magnon
phonon
RIXS and excited states
1000 eV
1 eV
100 meV
IR
UV/Vis

## Slide 3
Ψ0
Core level
electronic
dd, CT
magnon
phonon
RIXS and excited states
1000 eV
1 eV
100 meV
(Resonant) Raman

## Slide 4
Ψ0
Core level
electronic
dd, CT
magnon
phonon
RIXS and excited states
1000 eV
1 eV
100 meV
(Resonant) X-ray Raman

## Slide 5
Ψ0
Core level
electronic
dd, CT
magnon
phonon
RIXS and excited states
1000 eV
1 eV
100 meV
(Resonant) X-ray Raman
RIXS Resonant Inelastic X-ray Scattering
R-XES
Resonant X-ray Emission Spectroscopy

## Slide 6
Resonant Inelastic X-ray Scattering

## Slide 7
Resonant Inelastic X-ray Scattering
Energy
Polarization
Momentum
Eout ,kout, eout
Ein, kin, ein
q = kin - kout
h𝝎= Ein - Eout
Eout, ,kout, eout
Ein,, kin, ein

## Slide 8
Ψ0
Core-valence (electronic) RIXS
2p
electronic
dd, CT
magnon
vibrations

## Slide 9
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
3d9
2D
2D5/2
2D3/2
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
ATOMIC

## Slide 10
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
3d9
2D
2D5/2
2D3/2
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
ATOMIC

## Slide 11
Atomic Multiplet Theory
Cu2+ 2p XAS (from 3d9 to 2p53d10)
3d9
2D
2D5/2
2D3/2
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
Only L3 edge
ATOMIC

## Slide 12
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
3d9
2D
2D5/2
2D3/2
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
Only L3 edge
Spin-orbit excitation
Elastic line in 2p3d RIXS
ATOMIC

## Slide 13
Octahedral crystal field splitting
metal ion
in free space
in symmetrical field
t2g
yz xz xy
eg
in octahedral ligand field
x2-y2 z2
x2-y2 yz z2 xz xy
CRYSTAL FIELD EFFECT
3d1
2D
2Eg
2T2g

## Slide 14
Octahedral crystal field splitting
CRYSTAL FIELD EFFECT
3d9
2D
2D5/2
2D3/2
2T2g (1)
2T2g (2)
2Eg

## Slide 15
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
Crystal field excitations
Elastic line in 2p3d RIXS
OCTAHEDRAL
3d9
2D
2D5/2
2D3/2
2T2g (1)
2T2g (2)
2Eg

## Slide 16
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
Crystal field mixes J states
Both L3 and L2 edges
Crystal field excitations
Elastic line in 2p3d RIXS
OCTAHEDRAL
3d9
2D
2D5/2
2D3/2
2T2g (1)
2T2g (2)
2Eg

## Slide 17
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
OCTAHEDRAL
3d9
2D
2D5/2
2D3/2
2T2g (1)
2T2g (2)
2Eg

## Slide 18
Ψ0
Core-core RIXS
2p
electronic
dd, CT
magnon
vibrations
3s

## Slide 19
Resonant Inelastic X-ray Spectroscopy
2p XAS of CaF2
3d0

’
3s13d1
2p53d1
2p3s RIXS of CaF2

## Slide 20
2p3s RIXS of CaF2
Ground state is 3d0
Excitation (i0) 3d0  (x) 2p53d1
Decay (x) 2p53d1  (f) 3s13d1
2p3s RIXS of CaF2

## Slide 21
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d0
1S
1S0
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0

## Slide 22
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS
2 3 7 8 5
Dipole selection rule:
ΔJ=T1
(cubic symmetry)

## Slide 23
Atomic Multiplet Theory
X-ray emission from 2p53d1 to 3s13d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3s13d1
1D
3D
1D2
3D1
3D2
T2
E
T2
E
T1
A2
T1
T2
3D3

## Slide 24
Atomic Multiplet Theory
X-ray emission from 2p53d1 to 3s13d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3s13d1
1D
3D
1D2
3D1
3D2
T2
E
T2
E
T1
A2
T1
T2
3D3
Dipole selection rule:
ΔJ=T1 * T1=T1+T2 +E +A1
7x7 matrix

## Slide 25
Phys. Rev. B.
53, 7099 (1996)
Resonant Inelastic X-ray Scattering
3d0

’
3s13d1
2p53d1
2p3s RIXS of CaF2

## Slide 26
Ψ0
1s2p RIXS of transition metal ions
1s
electronic
dd, CT
magnon
vibrations
2p

## Slide 27: Pre-edge and edge
Only quadrupole peaks visible
3d7  1s13d8  2p53d8
CoO
high-spin CoII
3d7 [4T2]
Sharper pre-edge structures in 1s XAS

## Slide 28
K edge and 1s2p RIXS
Hard x-ray RIXS
Soft x-ray edges with hard x-rays
Reduce lifetime from 1.5 to 0.2 eV High Energy Fluorescence Detected (HERFD) XANES
Spin-polarized XAS
Range extended EXAFS
Background free FY for low concentrations
RIXS-MCD

## Slide 29
Co K edge of LiCoO2
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
K pre-edge of TM oxides (LiCoO2)
Remove lifetime broadening with HERFD

## Slide 30
Co K edge of LiCoO2
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
K pre-edge of TM oxides (LiCoO2)
Remove lifetime broadening with HERFD

## Slide 31
?
?
2p5d dipole
LaF3
2p4f quadrupole
4f0 2p5 4f1
Remove lifetime broadening with HERFD

## Slide 32
HERFD ≠ XAS
4f0 2p5 4f1  4d9 4f1

## Slide 33
free electron
3d band
valence band
core state
RIXS fluorescence
One-electron (level) Total energy (state)
RIXS fluorescence
core hole + electron
core excitons
dd excitation
phonon
ground state
valence hole + electron
RIXS and fluorescence
Notes: 33

## Slide 34
free electron
3d band
valence band
core state
RIXS fluorescence
One-electron (level) Total energy (state)
RIXS fluorescence
core hole + electron
core excitons
dd excitation
phonon
ground state
valence hole + electron
RIXS and fluorescence
Notes: 34

## Slide 35
Resonant Inelastic X-ray Scattering

## Slide 36
Resonant Inelastic X-ray Scattering
RIXS = XAS * XES
Fluorescence= XPS * XES

## Slide 37
2p3d RIXS
eV
electron-electron
crystal field
charge transfer
polarization, angles
(in, sample, out)
meV
spin-orbit, magnetic
distortions
vibrations
RIXS 2024: 8 meV
RIXS1998: 500 meV
Notes: 37

## Slide 38
[CoIIW12O40]·
[Van Schooneveld, Hunault et al., unpublished ]
2p3d RIXS of isolated chromium ions (ruby)

## Slide 39
Multiplet challenge: 2p3d RIXS on Cr3+
Notes: 39

## Slide 40
Resonant Inelastic X-ray Scattering
Energy
Polarization
Momentum
Eout ,kout, eout
Ein, kin, ein
q = kin - kout
h𝝎= Ein - Eout
Eout, ,kout, eout
Ein,, kin, ein

## Slide 41
Spin state of LaCoO3
[Wang et al. 2018 ]
q-dep. RIXS
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 42
Spin state of LaCoO3
[Wang et al. 2018 ]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 43
2p3d RIXS of transition metal ions

## Slide 44
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
3d9
2D
2D5/2
2D3/2
Dipole selection rule:
ΔJ=-1, 0 or +1
J=J’≠0
2p5
2P
2P3/2
2P1/2
Only L3 edge
Spin-orbit excitation
Elastic line in 2p3d RIXS
ATOMIC

## Slide 45
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
[Phys. Rev. B. 57, 14584 (1998)]
3d orbitals
2p orbitals

## Slide 46
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
[Phys. Rev. B. 57, 14584 (1998)]

## Slide 47
Atomic Multiplet Theory
Cu2+ 2p3d RIXS (from 3d9 to 2p53d10 to 3d9)
[Phys. Rev. B. 57, 14584 (1998)]

## Slide 48
Magnon 2p3d RIXS in cuprates

## Slide 49
NiII 3d8 []  2p53d9[jj]  3d8[]
2p3d RIXS of NiO
Notes: Cartoon of a spin-flip transition

## Slide 50
dd
spin-flip
‘spin-flip’
MS
S
2p3d RIXS of NiO
[Phys. Rev. B. 57, 14584 (1998)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 51
2p3d RIXS of NiO
[Phys. Rev. Lett. (2020)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 52
2p3d RIXS of NiO
[Phys. Rev. Lett. (2020)]
Notes: Low-loss region of RIXS in NiO.
Ground state: 3A2
Double group: T2, not split without exchange
Echange field H splits ground state into three Ms states as H times Ms,
So three states at –H, 0, +H.
The spin-flip peak in the figure is at 2H.
H is related to the superexchaneg energy

## Slide 53
2p3d RIXS of Fe2O3

## Slide 54
0,1 and 2-magnons in 2p3d RIXS of Fe2O3

## Slide 55
0,1 and 2-magnons in 2p3d RIXS of Fe2O3

## Slide 56
0,1 and 2-magnons in 2p3d RIXS of Fe2O3

## Slide 57
0,1 and 2-magnons in 2p3d RIXS of Fe2O3

## Slide 58
3-magnons in 2p3d RIXS of Fe2O3

## Slide 59
3-magnons in 2p3d RIXS of Fe2O3

## Slide 60
2p3d RIXS
eV
electron-electron
crystal field
charge transfer
polarization, angles
(in, sample, out)
meV
spin-orbit, magnetic
distortions
vibrations
RIXS 2024: 8 meV
RIXS1998: 500 meV
Notes: 60

## Slide 62
Electron yield
Fluorescence Yield (1. dilute limit)
FY (2. state dependent decay)
No XMCD sum rules in FY
FY (3. inverse PFY)
FY (4. dips and peaks)
Yield detection

## Slide 63
X-ray enters sample
Total absorption
Penetration depth λ is inverse proportional to
Yield detection
λ

## Slide 64
Core hole decays by photons (σ) or electrons (σE)
Electrons escape from surface determined by their kinetic energy λ
Electron yield: EY = * σE * λ ~
[Neglect angular dependences]
Electron Yield detection
λ
λ

## Slide 65
Electron Yield detection

## Slide 66
Core hole decays by photons (σ) or electrons (σE)
Photons escape prop. to λ’≈ ]
Fluorescence yield: FY = * σ * λ
[Neglect angular dependences]
Fluorescence Yield detection
λ

## Slide 67
Fluorescence yield: FY = * σ * λ
= +
λ ~1/
σ is different for edge and background (σB)
Fluorescence Yield detection
ITFY ~

## Slide 68
FY detection of dilute sample
ITFY ~
ITFY ~
ITFY ~

## Slide 69
FY detection of concentrated (bulk) sample
ITFY ~
Non-d
ITFY ~
“saturation & self-absorption”
De-saturation software
(μ(ω) based on CRXO)

## Slide 70
Single synchrotron pulselength is too long
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
XAS of radiation sensitive sample
Notes: 70

## Slide 71
FY-XAS of radiation sensitive sample
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Fluorescence does not measure XAS spectrum
Saturation ?
Notes: 71

## Slide 72
FY-XAS of radiation sensitive sample
Fluorescence does not measure XAS spectrum
NO Saturation
State-dependent decay
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 72

## Slide 73
Yield methods assume a constant ratio between radiative and non-radiative decay
If this ratio is state (= energy) dependent then the related yield methods do not measure XAS.
FY detection: State dependent decay

## Slide 74
FY detection: State dependent decay
FY
EY
L3
L2
Solid State Comm. 92, 991 (1994)

## Slide 75
The dominant yield method is not visibly affected, thus for soft X-rays only FY is affected, not electron yield.
FY detection: State dependent decay

## Slide 76
FY detection (state-dependent, dilute)
ITFY ~
ITFY ~
Main decay of 2p core hole is 2p3d RIXS
Integrate RIXS spectrum to 2p3d PFY
TFY ~ 2p3d PFY
NOTE: “RIXS” has angular dependence effects

## Slide 77
XAS: transmission & FY
Mitzner et al, J. Phys. Chem. Lett. 4, 3641 (2013)
Notes: 77

## Slide 78
FY-XAS ≠ XAS L2 edge increases High-energies increase
Fluorescence Yield detection
Kurian J. Phys. Cond. Matt. 24, 435602 (2012)

## Slide 79
XMCD sum rules break down
Ni/Co 20%, Fe 30%, Mn > 100% error
Fluorescence Yield XMCD
Liu, Phys. Rev. B. 96, 054446 (2017)

## Slide 80
ITFY ~ = the integrated RIXS
Measure the partial fluorescence yield of the background.
IBFY ~
1/(1+x) ≈ 1 – x
IBFY ≈ 1 –
Measure a negative XAS spectrum, essentially tracking the probing depth [λ]
FY detection: 3 inverse PFY

## Slide 81
FY detection: 3 inverse PFY
Achkar ea, scientific reports 1, 82 (2011)

## Slide 82
FY detection: 4 dips and peaks
Measure the total fluorescence yield
State-dependent metal PFY + IPFY
ITFY ~
ITFY ~ c1

## Slide 83
FY detection: 4 dips and peaks
Nature Chem. 4, 766 (2012) & Phys. Rev. Letter discussions (2014)