## Slide 1
Introduction to XAS
XAS spectral shape (oxygen K edge)
Charge transfer (core hole screening)
XPS spectral shape
XAS spectral shape (metal K edge)
Core hole decay & detection techniques
Overview of core hole spectroscopies
XAS with charge transfer multiplets
X-ray Absorption Spectroscopy

## Slide 2
Element specific
Sensitive to low concentrations
Applicable under extreme conditions
SPACE: Combination with x-ray microscopy
TIME: femtosecond XAS
RESONANCE: RIXS, RPES, R diffraction
X-ray Absorption Spectroscopy
Notes: XAS is element specific because each element has specific binding energies for its core levels.
The XAS edge energy is essentially given by the core level binding energy.

## Slide 3: Interaction of x-rays with matter
The photon moves towards the atom
Interaction of x-rays with matter

## Slide 4: Interaction of x-rays with matter
The photon is scattered by an electron
Interaction of x-rays with matter
X-ray scattering X-ray diffraction
X-ray scattering is independent of the x-ray energy

## Slide 5: Interaction of x-rays with matter
The photon is scattered by an electron
Interaction of x-rays with matter
X-ray scattering X-ray diffraction

## Slide 6: Interaction of x-rays with matter 1
The photon meets an electron and is annihilated
Interaction of x-rays with matter

## Slide 7: Interaction of x-rays with matter
The electron gains the energy of the photon and is turned into a blue electron.
Interaction of x-rays with matter

## Slide 8: Interaction of x-rays with matter
The blue electron (feeling lonely) leaves the atom
Interaction of x-rays with matter

## Slide 9: Interaction of x-rays with matter
The probability of photon annihilation determines
the intensity of the transmitted photon beam
I0
I (XAS)
Ek (XPS)
Interaction of x-rays with matter

## Slide 10: Interaction of x-rays with matter
XAS, XPS
Elastic scattering (SAXS, XRD)
Inelastic scattering
Mn
X-ray absorption

## Slide 11
Label
Orbital
eV
K
1s
6539
L I
2s
769
L II
2p1/2
650
L III
2p3/2
639
M I
3s
82
M II
3p1/2
47
M III
3p3/2
47
X-ray absorption edges
X-ray Absorption Spectroscopy

## Slide 12
Label
Orbital
eV
K
1s
6539
L I
2s
769
L II
2p1/2
650
L III
2p3/2
639
M I
3s
82
M II
3p1/2
47
M III
3p3/2
47
X-ray absorption edges
X-ray Absorption Spectroscopy
BarKLa
The Nobel Prize in Physics 1917 was awarded to Charles Glover Barkla "for his discovery of the characteristic Röntgen radiation of the elements."

## Slide 13
Label
Orbital
eV
K
1s
6539
L I
2s
769
L II
2p1/2
650
L III
2p3/2
639
M I
3s
82
M II
3p1/2
47
M III
3p3/2
47
X-ray absorption edges
X-ray Absorption Spectroscopy
BarKLa
The Nobel Prize in Physics 1917 was awarded to Charles Glover Barkla "for his discovery of the characteristic Röntgen radiation of the elements."
sharp
principal
diffuse
fundamental
J. Chem. Educ. 84, 757 (2007)

## Slide 14
X-ray Absorption Spectroscopy
Atomic electronic structure X-ray absorption of an atom
E = - Z2/n2 * 13.6 eV

## Slide 15
X-ray Absorption Spectroscopy
Atomic electronic structure X-ray absorption of an oxygen atom
(Rydberg states)

## Slide 16
X-ray Absorption Spectroscopy
Molecular electronic structure X-ray absorption of an O2 molecule
(σ* mixed with Rydberg states)

## Slide 17
Introduction to XAS
XAS spectral shape (oxygen K edge)
Charge transfer (core hole screening)
XPS spectral shape
XAS spectral shape (metal K edge)
Core hole decay & detection techniques
Overview of core hole spectroscopies
XAS with charge transfer multiplets
X-ray Absorption Spectroscopy

## Slide 18
4sp
Eg
T2g
O2p
O2s
O 1s ~530 eV
XAS: spectral shape (O 1s)
Electronic structure of a transition metal oxide
Main bonding:
O2p with metal 4sp
Gives valence band and conduction band,
Mixed in character
Additional bonding
O2p with metal 3d;
Gives mixed 3d bands split by crystal field in octahedral symmetry, T2g states have pi-bonding and Eg states have sigma-bonding.
oxygen 1s core state
is localized at an oxygen atom
Notes: 18

## Slide 19
4sp
Eg
T2g
O2p
O2s
O 1s ~530 eV
XAS: spectral shape (O 1s)
transition from oxygen 1s state
to an empty state
oxygen 1s core state
is localized at an oxygen atom
local empty DOS
dipole selection rule:
p-projected DOS
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
[Phys. Rev. B. 40, 5715 (1989); review in Chem. Rev. 120, 4056 (2020)]
Notes: 19

## Slide 20
2p
2s
Phys. Rev. B.40, 5715 (1989)
XAS: spectral shape (O 1s)

## Slide 21
Electronic Structure: TiO2
XAS: spectral shape
E
T2
TiO2: 3d0
E
T2
Cr2O3: 3d3

## Slide 22
Electronic Structure: TiO2
XAS: spectral shape
E
T2
TiO2: 3d0
E
T2
Cr2O3: 3d0
4 >6
6
2 >3
5 >6

## Slide 23
Phys. Rev. B.40, 5715 (1989); 48, 2074 (1993)
XAS: spectral shape (O 1s)
oxygen 1s > p DOS

## Slide 24
Final State Rule: Spectral shape of XAS looks like final state DOS
TiSi2
Phys. Rev. B. 41, 11899 (1991)
XAS: spectral shape
Lecture Amelie Juhin

## Slide 25
XAS: spectral shape (O 1s)
Crystal structure
Electronic structure calculation, for example Density Functional Theory (DFT)
(in the presence of the core hole)
Calculation of the oxygen
p-projected local empty DOS
Compare with experiment
CODES: FEFF, Wien2K, VASP, QE, etc.

## Slide 26
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
XAS: spectral shape (Ti 2p)
Expect the d (and s-) projected Ti DOS
Why is experiment different?
2p > 3d
Notes: 26

## Slide 27
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
XAS: spectral shape (Ti 2p)
Expect the d (and s-) projected Ti DOS
2p spin-orbit coupling (~6 eV)
2p > 3d
Notes: 27

## Slide 28
4sp
Eg
T2g
O2p
O2s
Ti 2p ~460 eV
XAS: spectral shape (Ti 2p)
Expect local d-projected Ti DOS
Core spin-orbit splitting
Overlap of core 2p and valence 3d states
>> many electron excitations dominate
2p3d 2-electron integrals
Notes: 28

## Slide 29
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
IXAS = |< 2p5 3d1 |dipole| 3d0>|2 [E=0]
Single electron (excitation) approximation breaks down :
IXAS = |<3d |dipole| 2p>|2 
X-ray absorption
XAS: spectral shape (Ti 2p)
Can NOT approximate 2p-3d interaction as extra potential
Large core hole spin-orbit coupling

## Slide 30
Fermi Golden Rule:
IXAS = |<f|dipole| i>|2 [E=0]
IXAS = |< 1s1 2p5 |dipole| 2p4>|2 [E=0]
Single electron (excitation) approximation :
IXAS = |<2p |dipole| 1s>|2 
X-ray absorption
XAS: spectral shape (O 1s)
Can neglect local 2p-2p interaction
Can approximate 1s-2p interaction as extra potential
No core hole spin-orbit coupling

## Slide 31: XAS
Single Particle:
1s edges
(DFT codes, TD-DFT)
Total energy:
2p, 3s, 3p edges
(Multiplet codes)
XAS: two models

## Slide 32
Introduction to XAS
XAS spectral shape (oxygen K edge)
Charge transfer (core hole screening)
XPS spectral shape
XAS spectral shape (metal K edge)
Core hole decay & detection techniques
Overview of core hole spectroscopies
XAS with charge transfer multiplets
X-ray Absorption Spectroscopy

## Slide 33
Lecture Marie-Anne Arrio
Charge Transfer Multiplet program
Used for the analysis of XAS, EELS,
Photoemission, Auger, XES involving d and f-shells
ATOMIC INTERACTIONS

CRYSTAL FIELD

CHARGE TRANSFER
CHARGE TRANSFER MULTIPLETS
Notes: The TT-multiplets program can be used to explain the spectral shapes of all core level spectroscopies. XAFS, photoemission, auger, etc.
The program combines three advanced computer codes, an atomic physics code to describe all atomic interactions, a group theory code to describe the local symmetry (think of crystal fields) and model Hamiltonians to describe many body effects correlated systems.
AS A SIDE REMARK I WOULD LIKE TO MENTION that the active site in a catalyst is a perfect example of a correlated system. (in biocatalysis this is often realised)
The integrated program gives accurate descriptions of core level spectra, from a set of uniform electronic structure parameters.
The program is important for all of the new spectroscopies that I will describe.
The program is distributed from my homepage and it is used at some 50 institutes worldwide.

## Slide 34
valence e-e interactions Fdd
core-valence e-e Fpd Gpd
core & valence spin-orbit ζ
crystal field 10Dq, Ds, Dt
molecular field, M or H
e-e screening κ
charge transfer Δ, U, Q
hopping TΓ
ionic 3d
4f, 5f
atomic 3d
covalent 3d
mixed valence f
ATOMIC
SYMMETRY
BONDING
Multiplet calculations

## Slide 35
Hubbard U for a 3d8 ground state:
U= E(3d7) + E(3d9) – E(3d8) – E(3d8)
Ligand-to-Metal Charge Transfer (LMCT):
= E(3d9L) – E(3d8)
Charge Transfer Effects
Charge transfer effects

## Slide 36
Charge Transfer Effects
Main screening mechanism in XAS of oxides:
Ligand-to-metal charge transfer
Charge transfer energy  is important for XAS
Hubbard U is NOT important for XAS spectral shape
Charge transfer effects

## Slide 37
3d9L
Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

3d8
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects

## Slide 38

Charge Transfer Effects
3d8
3d9L
Charge transfer effects

## Slide 39

Charge Transfer Effects
3d8
3d9L
9
8
Charge transfer effects

## Slide 40
β 3d8 - α 3d9L
α 3d8 + β 3d9L

Charge Transfer Effects
3d8
3d9L
Charge transfer effects

## Slide 41
E1,2 = ½ [±√(2+4T2)]
=2 and T=0
E1,2 = ½ [2±√(22+0)] = 0 and 2

Charge Transfer Effects
3d8
3d9L
Charge transfer effects

## Slide 42
E1,2 = ½ [±√(2+4T2)]
=2 and T=1
E1,2 = ½ [2±√(22+4)] = 1 ± √2

Charge Transfer Effects
3d8
3d9L
Charge transfer effects

## Slide 43
Charge Transfer Effects in NiO
E(3d9L) – E(3d8) = 
E(3d10LL‘) – E(3d8) = 2
X
Charge transfer effects

## Slide 44
Charge Transfer Effects in NiO
E(3d9L) – E(3d8) = 
E(3d10LL‘) – E(3d8) = 2 +U
Charge transfer effects

## Slide 45
Charge Transfer Effects
Charge transfer effects

## Slide 46

+U-Q
Charge Transfer Effects in XAS
Charge transfer effects

## Slide 47
3d9L
3d8
NiO: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

2p53d10L
2p53d9
+U-Q  
Charge Transfer Effects
Charge transfer effects

## Slide 48
β 3d8 - α 3d9L
α 3d8 + β 3d9L

+U-Q  
β’ c3d9 – α’ c3d10L
α' c3d9 + β’ c3d10L
~0
~1
Intensity bonding combination: [α α’+ β β’]2
α  α’  (α2+ β2)2 =1
Charge transfer effects

## Slide 49
β 3d5 - α 3d6L
α 3d5 + β 3d6L

+U-Q  
β’ c3d6 – α’ c3d7L
α' c3d6 + β’ c3d7L
~0
~1
Intensity anti-bonding combination: [α β’- β α’]2
α  α’  (αβ – βα)2 =0
Charge transfer effects

## Slide 50
Neutral experiments are self-screened
XAS, optical, EPR, EELS, RIXS
>> small screening satellites
>> crystal field theory can be used
Ionising experiments are not self-screened
XPS, Auger,
>> large screening > large satellites
>> crystal field theory can not be used
Charge Transfer Effects
Charge transfer effects

## Slide 51
3d6L
Transition metal oxide: Ground state: 3d5 + 3d6L
Energy of 3d6L: Charge transfer energy 
XAS
2p53d7L
+U-Q  

2p53d6
3d5
2p53d6L
XPS
2p53d5
-Q
Ground State
Charge transfer effects in XAS and XPS
Charge transfer effects in XAS and XPS

## Slide 52
Introduction to XAS
XAS spectral shape (oxygen K edge)
Charge transfer (core hole screening)
XPS spectral shape
XAS spectral shape (metal K edge)
Core hole decay & detection techniques
Overview of core hole spectroscopies
XAS with charge transfer multiplets
X-ray Absorption Spectroscopy

## Slide 53
Charge transfer
Charge transfer effects in XAS
XAS = neutral
Self screened
Small charge transfer satellites

## Slide 54

+U-Q
Charge Transfer Effects in XAS
Charge transfer effects in XAS

## Slide 55

-Q
Charge Transfer Effects in XPS
Charge transfer effects in XPS

## Slide 56
Charge transfer effects in XPS
Charge transfer effects in XPS
XAS = neutral
Self screened
Small charge transfer satellites
XPS = ionising
Large screening
Large charge transfer satellites

## Slide 57
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 58
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 59
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3

## Slide 60
Charge transfer effects in XPS
1s and 2p XPS of Fe2O3
LDA + DMFT:
Use actual DMFT-based band structure
result to couple to the localised states
More on Thursday/friday
Phys. Rev. B.100, 075146 (2019)

## Slide 61
Introduction to XAS
XAS spectral shape (oxygen K edge)
Charge transfer (core hole screening)
XPS spectral shape
XAS spectral shape (metal K edge)
Core hole decay & detection techniques
Overview of core hole spectroscopies
XAS with charge transfer multiplets
X-ray Absorption Spectroscopy

## Slide 62: XAS
Single Particle:
1s edges
(DFT codes, TD-DFT)
Total energy:
2p, 3s, 3p edges
(Multiplet codes)
XAS: two models

## Slide 63
Iron 1s XAS
[J. Phys. Chem. B. 109, 20751 (2005)]
exciton
edge jump
Metal K edges: dipole & quadrupole
3d systems
1s > p dipole
1s > 3d quadrupole
Notes: 63

## Slide 64
3d
N
4p
0
1s
1
3d
N+1
4p
0
pre-edge
edge
1s
1
3d
N
4p
1
pre-edge (interpretation)

## Slide 65
3d
N
4p
0
1s
1
3d
N+1
4p
0
pre-edge
edge
1s
1
3d
N
4p
1
[J. Phys. Cond. Matt. 21, 104207 (2009)]
pre-edge (interpretation)

## Slide 66
CoIII(acac)
K edge and 1s2p RIXS
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
1s2p RIXS of transition metal ions

## Slide 67
Co K edge of LiCoO2
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
K pre-edge of TM oxides (LiCoO2)
Pre-edges structures in 1s XAS

## Slide 68
Co K edge of LiCoO2
low-spin CoIII
3d6 [1A1]
T2g full
Eg empty
K pre-edge of TM oxides (LiCoO2)
Pre-edges structures in 1s XAS

## Slide 69
K pre-edge of TM oxides
Pre-edges structures in 1s XAS
J. Phys. Cond. Matt. 21, 104207 (2009); Phys. Rev. B. 81, 115115 (2010)

## Slide 70
K edge and 1s2p RIXS
K main edge (interpretation)
K main edge (+non-local peaks) calculated
from transitions to empty states
Calculated with TD-DFT/BSE, for example:
  Exciting, Ocean
Calculated with DFT, for example:
  Multiple scattering (FEFF, FDMNES)
  Band structure (Wien2K, VASP, QuantumEspresso)
  Molecular DFT (ADF, ORCA)

## Slide 71
K edge and 1s2p RIXS
K main edge (interpretation)
a
d
K main edge calculated from transitions to empty states
[Juhin PRB 81, 115115 (2010)]
LiCoO2
LDA+U + Q

## Slide 72
K main edge (interpretation)
[Ghiasi et al., PRB 100, 075146 (2019)]
1s XPS spectrum of NiO has multiple peaks
One photon energy relates to many different electron kinetic energies:

## Slide 73
K main edge (interpretation)
[Ghiasi et al., PRB 100, 075146 (2019)]
1s XPS spectrum has multiple peaks
One photon energy relates to many different electron kinetic energies:
One cannot do XAS calculations with a single kinetic energy
1s XAS does NOT look (exactly) like the empty DOS

## Slide 74
Introduction to XAS
XAS spectral shape (oxygen K edge)
Charge transfer (core hole screening)
XPS spectral shape
XAS spectral shape (metal K edge)
Core hole decay & XAS detection
Overview of core hole spectroscopies
XAS with charge transfer multiplets
X-ray Absorption Spectroscopy

## Slide 75
X-ray absorption & Auger
    Auger decay
    X-ray emission
X-ray Absorption Spectroscopy
Notes: 75

## Slide 76
X-ray Absorption Spectroscopy
1s core state
Soft x-rays: Auger
Hard x-rays: fluorescence
Notes: 76

## Slide 77
XAS: detection techniques

## Slide 78
Use decay channels as detector
XAS: detection techniques
Uniform thickness
Uniform concentration of absorbing element
Thin enough for photons

## Slide 79
X-ray penetration lengths &
electron escape depths
100-1000 nm
(CXRO, but 20 nm for L edges)
1-5 nm
XAS: detection techniques

## Slide 80
Use decay channels as detector
XAS: detection techniques
X-ray penetrate 1000 nm (λX)
Electrons escape from 5 nm (λE)
Number of core holes created in first 5 nm is proportional to μ
ITEY ~ 1 / λX = μX

## Slide 81
Transmission
(pinhole, saturation > thin samples)
Electron Yield
(surface sensitive)
Fluorescence Yield
(saturation & self-absorption:
> dilute samples)
[L edges are intrinsically distorted]
XAS: detection techniques

## Slide 82
Introduction to XAS
XAS spectral shape (oxygen K edge)
Charge transfer (core hole screening)
XPS spectral shape
XAS spectral shape (metal K edge)
Core hole decay & XAS detection
Overview of core hole spectroscopies
XAS with charge transfer multiplets
X-ray Absorption Spectroscopy

## Slide 83
Write down all core level spectroscopies
Excitation
Decay
Resonances/scattering
Notes: The TT-multiplets program can be used to explain the spectral shapes of all core level spectroscopies. XAFS, photoemission, auger, etc.
The program combines three advanced computer codes, an atomic physics code to describe all atomic interactions, a group theory code to describe the local symmetry (think of crystal fields) and model Hamiltonians to describe many body effects correlated systems.
AS A SIDE REMARK I WOULD LIKE TO MENTION that the active site in a catalyst is a perfect example of a correlated system. (in biocatalysis this is often realised)
The integrated program gives accurate descriptions of core level spectra, from a set of uniform electronic structure parameters.
The program is important for all of the new spectroscopies that I will describe.
The program is distributed from my homepage and it is used at some 50 institutes worldwide.

## Slide 84
3d8 + ω
2p53d9
XAS1
X-ray spectroscopies

## Slide 85
3d8 + ω
2p53d9
2p53d8+e’
XAS1
XPS2
X-ray spectroscopies

## Slide 86
3d8 + ω
2p53d9
2p53d8+e’
XAS1
XPS2
XES3
RIXS5
3d8 + ω’
X-ray spectroscopies
IXS8

## Slide 87
3d8 + ω
2p53d9
2p53d8+e’
3d7 + e’
XAS1
XPS2
3p43d9+e’
XES3
RIXS5
AES4
3d8 + ω’
RAES6
RPES7
X-ray spectroscopies
IXS8

## Slide 88
3d8 + ω
2p53d9
2p53d8+e’
3d7 + e’
XAS1
XPS2
3p43d9+e’
XES3
RIXS5
AES4
3d8 + ω’
RAES6
RPES7
XES
XES
3d7 +e’+ω’
X-ray spectroscopies
IXS8

## Slide 89
3d8 + e
2p53d10
APS
Electron spectroscopies

## Slide 90
3d8 + e
2p53d10
APS
Electron spectroscopies
XES
RIPES
3d9 + ω’

## Slide 91
3d8 + e
2p53d10
APS
Electron spectroscopies
XES
RIPES
3d9 + ω’
3d8+e’
AES
REELS

## Slide 92
3d8 + e
2p53d10
APS9
Electron spectroscopies
XES
RIPES10
3d9 + ω’
3d8+e’
AES
REELS11
EELS12

## Slide 93
 | absorption | ω' | e'
x-ray (ω) | XAS |  | 
electron (e) |  |  | 
3d5 + ω
2p53d6
XAS
[Phys. Rev. B. 42, 5459 (1990)]
X-ray Absorption Spectroscopy

## Slide 94
 | absorption | ω' | e'
x-ray (ω) | XAS | (R)IXS | 
electron (e) |  |  | 
3d7 + ω
2p53d8
XAS
XES
RIXS
=XAS*XES
3d7 + ω’
IXS
[van Schooneveld et al., J. Phys. Chem. C. 116, 15218 (2012)]
Resonant Inelastic X-ray Scattering

## Slide 95
 | absorption | ω' | e'
x-ray (ω) | XAS | (R)IXS | (R)PES
electron (e) |  |  | 
3d8 + ω
2p53d9
XAS
AES
R-PES
=XAS*AES
(R-AES)
XPS
[Finazzi et al., Phys. Rev. B. 59, 9933 (1999)]
3p53d8+e’
Resonant
Photoemission

## Slide 96
 | absorption | ω' | e'
x-ray (ω) | XAS | (R)IXS | (R)PES
electron (e) | APS |  | 
3d8 + e
2p53d10
APS
[Fukoda et al., J. Appl. Phys. 106, 023701 (2009)]
Appearance Potential Spectroscopy

## Slide 97
 | absorption | ω' | e'
x-ray (ω) | XAS | (R)IXS | (R)PES
electron (e) | APS | (R)IPES | 
4f1 + e
3d94f3
APS
[Tanaka&Jo, JPSJ. 65, 615 (1995)]
XES
4f2 + ω’
IPES
RIPES
=APS*XES
Resonant Inverse Photoemission

## Slide 98
 | absorption | ω' | e'
x-ray (ω) | XAS | (R)IXS | (R)PES
electron (e) | APS | (R)IPES | (R)EELS
3d8 + e
2p53d10
APS
AES
R-EELS
=APS*AES
EELS
[Gorschluter et al., J. Elec. Spec 87, 211 (1998)]
3d8+e’
NiO
Resonant Electron Energy Loss

## Slide 99
 | absorption | ω' | e'
x-ray (ω) | XAS | (R)IXS | (R)PES
electron (e) | APS | (R)IPES | (R)EELS

## Slide 100
Resonant spectroscopies
RIXS (ω,ω’)
RAES (ω,e’)
RPES (ω,e’)
XES (ω’,e’)
RIPES (e,ω’)
REELS (e,e’)
(+ coincidence) (+ polarization) (+ momentum)
(+ time, space, cascade)
X-ray in (ω)
X-ray out (ω’)
RIXS

## Slide 101
Introduction to XAS
XAS spectral shape (oxygen K edge)
Charge transfer (core hole screening)
XPS spectral shape
XAS spectral shape (metal K edge)
Core hole decay & XAS detection
Overview of core hole spectroscopies
XAS with charge transfer multiplets
X-ray Absorption Spectroscopy

## Slide 102
XAS: spectral shape
1s XAS: K edges
Calculation of the
p-projected local empty DOS (FEFF, Wien2K, VASP, QE, Ocean)
2p XAS: L edges
Calculation of the
final state with
charge transfer multiplets (CRISPY, CTM4XAS)

## Slide 103
Charge Transfer Multiplet program
Model Hamiltonians used for the analysis of XAS, EELS, XES, RIXS, XPS, Auger, RPES involving d and f-shells ATOMIC

CRYSTAL FIELD

CLUSTER

DMFT + IMPURITY
HAMILTONIANS USING MULTIPLETS
Notes: The TT-multiplets program can be used to explain the spectral shapes of all core level spectroscopies. XAFS, photoemission, auger, etc.
The program combines three advanced computer codes, an atomic physics code to describe all atomic interactions, a group theory code to describe the local symmetry (think of crystal fields) and model Hamiltonians to describe many body effects correlated systems.
AS A SIDE REMARK I WOULD LIKE TO MENTION that the active site in a catalyst is a perfect example of a correlated system. (in biocatalysis this is often realised)
The integrated program gives accurate descriptions of core level spectra, from a set of uniform electronic structure parameters.
The program is important for all of the new spectroscopies that I will describe.
The program is distributed from my homepage and it is used at some 50 institutes worldwide.

## Slide 104
2p XAS of TiO2
2p XAS of Ti4+ ions
Ground state of Ti4+ is 3d0
Dipole transition 3d02p53d1
Ground state symmetry: 1S0
Final state symmetry: 2P2D gives
1P, 1D, 1F, and 3P, 3D, 3F
Atomic multiplets: 2p XAS of Ti4+

## Slide 106
3d XAS of rare earths
4f electrons are localized
No effect of surroundings (crystal field < lifetime broadening)
3d XAS is self screened > no charge transfer effect
Initial state
electron-electron interaction.
Valence spin-orbit coupling
Final state
+ core hole – valence hole ‘multiplet’ interaction.
+ core hole spin-orbit coupling

## Slide 107
3d XAS of rare earths
Nd3+ 4f3 system: ground state is 4I9/2

## Slide 108
Octahedral crystal field splitting
metal ion
in free space
in symmetrical field
t2g
yz xz xy
eg
in octahedral ligand field
x2-y2 z2
x2-y2 yz z2 xz xy
CRYSTAL FIELD EFFECT
3d1
2D
2Eg
2T2g

## Slide 109
Atomic Multiplet Theory
CRYSTAL FIELD EFFECT
3dN
J=0
J=4
J=1
J=2
J=3
A1
T2
T1
E
A1
E
T2
A2
T2
T1
T1
    Branching rules:
    Same rules for any quantum number
    S, L or J

## Slide 110
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS

## Slide 111
Atomic Multiplet Theory
X-ray absorption from 3d0 to 2p53d1
2p53d1
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
3d0
1S
1S0
A1
ee LS CFS
2 3 7 8 5
Dipole selection rule:
ΔJ=T1
(cubic symmetry)

## Slide 112
Comparison with Experiment
2p XAS of ScF3 with crystal field multiplets
PHYS. Rev. B. 41, 928 (1990) [google drive]

## Slide 113
2p XAS of 3d transition metal oxides
3d electrons are less localized
Effect of surroundings (crystal field effect)
3d XAS is self screened > weak charge transfer effect
Initial state
electron-electron interaction.
valence spin-orbit coupling
crystal field effect
Final state
core hole – valence hole ‘multiplet’ interaction.
core hole spin-orbit coupling
crystal field effect

## Slide 114
Atomic Multiplet Theory
ATOMIC MULTIPLETS 3d8
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
electron-electron
Interaction
(~2 eV)
spin-orbit
coupling
(~50 meV)
    Ground state:
    Given by Hunds rules
    max S
    max L
    max J (if more than half full)

## Slide 115
Atomic Multiplet Theory
X-ray absorption from 3d8 to 2p53d9
2p53d9
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
Dipole selection rule:
ΔJ=-1, 0 or +1

## Slide 116
Atomic Multiplet Theory
X-ray absorption from 3d8 to 2p53d9
2p53d9
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
3d8
1S
3F
1G
3P
1D
1S0
3P2
1G4
3P1
3P0
3F4
3F2
3F3
1D2
Dipole selection rule:
ΔJ=-1, 0 or +1

## Slide 117
Atomic Multiplet Theory
X-ray absorption from 3d8 to 2p53d9
2p53d9
1P
3F
1D
3P
3D
1P1
3P2
1D2
3P1
3P0
3F4
3F2
3F3
3D3
1F
1F3
3D1
3D2
T1
T2
E
T2
E
T2
E
T2
E
T1
T1
A2
T1
T2
A2
T1
T2
A2
T1
T2
A1
A1
T1
T2
E
2 3 7 8 5
3F4
3d8
A1
3A2
T2
Atomic
crystal field
+ spin-orbit
dipole transition
T1
A2
T1
T2
E
x
=

## Slide 118
3d9L
3d8
NiO: Ground state: 3d8 + 3d9L
Energy of 3d9L: Charge transfer energy 

2p53d10L
2p53d9
+U-Q  
Charge Transfer Effects
Charge transfer effects

## Slide 119
Tanabe-Sugano with Charge transfer
α 3d8 + β 3d9L
Tanabe-Sugano diagrams with charge transfer
NiO
Cu3+

## Slide 120
=10
NiO
La2Li½Cu½O4
30% 3d8
1A1
30% 3d8
3A2
=-5
=5
=0
=-10
3d8 + 3d9L
Charge Transfer effects
Chem. Phys. Lett. 297, 321 (1998)
Charge transfer effects in XAS

## Slide 121
3d6L
3d5

2p53d7L
2p53d6
+U-Q  
FeIII: Ground state: 3d5 + 3d6L
LMCT and MLCT:  - bonding
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)

## Slide 122
3d4L
3d6L
3d5
FeIII: Ground state: 3d5 + 3d6L + 3d4L

2p53d5L
2p53d7L
2p53d6
+U-Q   - 2

-U+Q   + 2
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 123
FeIII(tacn)2
FeIII(CN)6
with Ed Solomon (Stanford) JACS 125, 12894 (2003),
JACS 128, 10442 (2006), JACS 129, 113 (2007)
LMCT and MLCT:  - bonding

## Slide 124
Introduction to XAS
XAS spectral shape (oxygen K edge)
Charge transfer (core hole screening)
XPS spectral shape
XAS spectral shape (metal K edge)
Core hole decay & XAS detection
Overview of core hole spectroscopies
XAS with charge transfer multiplets
X-ray Absorption Spectroscopy